## Slide 1: Stacking interactions – a broader perspective
Krešimir Molčanov, Biserka Kojić-Prodić
Rudjer Bošković Institute
Zagreb, Croatia

## Slide 2: KHCA∙2H2O
P 21/c
0
b
a
CrystEngComm, 2009, 11, 1407.

## Slide 3: KHCA∙2H2O
Centroid distance:
3.229(2) Å
Offset ≈ 0.2 Å
P 21/c
CrystEngComm, 2009, 11, 1407.
c

## Slide 4: Is it because of stacking?
c
CrystEngComm, 2015, 17, 8645.

## Slide 5: Common misconceptions
It occurs only between aromatic rings
It is a weak interaction (E < 1 kcal mol-1)
In crystal packing it plays a ‘second fiddle’ to stronger interactions such as hydrogen bonding
It can’t be used in crystal engineering

## Slide 6
Look, these coins stack!
That means gold is aromatic!
An amazing discovery,
your majesty! It could
win us an IgNobel prize!

## Slide 7: Types of π-interactions
Weak: dominantly dispersion, E < 5 kcal mol-1
Medium: dominantly electrostatic, E = 5 – 15 kcal mol-1
Strong: partially covalent, E > 15 kcal mol-1
Similar to stacking: π-hole interactions

## Slide 8: Weak interactions
Aromatic rings
Heteroaromatic rings
Strongly charged non-aromatic rings (e.g. chloranilate dianions)
Dominantly dispersion, E < 5 kcal mol-1
Almost all studied examples

## Slide 9
Typical centroid
distance:
> 3,8 Å
Offset typically
1,7 – 1,8 Å
Hunter & Sanders, JACS, 1990, 112, 5525.
Hunter, Singh, Thornton, J. Mol. Biol, 1991, 208, 837.
Stacking of aromatic rings
Attraction
Repulsion
offset
α

## Slide 10
δ+
δ+
δ-
δ-
σ∙∙∙π attraction
π∙∙∙π repulsion
σ∙∙∙π attraction
Aromatic π-interactions:
quadrupolar moments

## Slide 11: Rethinking the term „pi-stacking”
Martinez & Iverson, Chem. Sci., 2012, 3, 2191.

## Slide 12
No attractive interactions:
N-methylpyridinium cations
Cg…Cg = 3.776(2) Å
CgI_perp = 3.766(2) Å
α = 0°
β = 4.2°
Offset = 0.279 Å
ρmax = 0.018 e Å-1
Cryst. Growth Des., 2019, 19, 391-402.

## Slide 13
Weak interactions:
tetrachlorohydroquinone
ρmax = 0.034 e Å-1
3.50 Å
3.55 Å
Cg…Cg = 4.7740(9) Å
CgI_perp = 3.3957(2) Å
α = 0.00(2)°
β = 44.7°
Offset = 3.356 Å
Cryst. Growth Des., 2019, 19, 391-402.

## Slide 14: Medium strong interactions
2,5-dihydroxyquinonate monoanions
Other non-aromartic rings
Metal-chelate rings
Dominantly electrostatic, E = 5 – 15 kcal mol-1

## Slide 15: Quinoid rings: no more quadrupoles
Cryst. Growth Des., 2019, 19, 391-402; 2019, 19, 2801-2810.

## Slide 16: Quinone anions: hydrogenchloranilate
CrystEngComm, 2015, 17, 8645.
ρmax = 0.059 e Å-1
E > 10 – 15 kcal mol-1
3.229(2) Å

## Slide 17
HCA-
HBA-
Effect of substituents
DHQ2-
CrystEngComm, 2013, 15, 135-143.

## Slide 18: Metal-chelate rings: aromatic?
RSC Adv., 2016, 6, 62785-62796.
[Cu(CA)2(H2O)2]Him2

## Slide 19: Metal-chelate rings: aromatic?
Cu1-O1
ρtot = 0.33 e Å-3
Laplacian = 5.87
Cu1-O2
ρtot = 0.36 e Å-3
Laplacian = 6.11
Cu-O bond critical points (3,-1):
Laplacian of electron density
Cryst. Growth Des., 2019, 19, 2801-2810.

## Slide 20: Stacking of metal-chelate rings in [Cu(CA)(2,2’-bpy)]
0
a
c
b
Dalton Trans., 2013, 42, 15756-15765.
3.28 Å

## Slide 21: Stacking of metal-chelate rings: electrostatic potential
IUCrJ, 2019, 6, 156-166.
Dalton Trans., 2013, 42, 15756-15765.

## Slide 22: Stacking of metal-chelate rings: Voronoi-Dirichlet polyhedra
IUCrJ, 2019, 6, 156-166.
Dalton Trans., 2013, 42, 15756-15765.

## Slide 23: π-Stacking of the coordination polymers: [Cu(CA)(MeCN)]n
RSC Adv., 2016, 6, 62785-62796.
3.26 Å
offset:
≈ 1.6 Å

## Slide 24: π-Stacking of the coordination polymers: [Cu(CA)(MeCN)]n
IUCrJ, 2019, 6, 156-166.
RSC Adv., 2016, 6, 62785-62796.

## Slide 25: Stacking or bonding? [Cu(CA)(1,10’-phen)]
0
a
c
b
2.574(2) Å
≈ 3.2 Å
Dalton Trans., 2014, 43, 7208-7218.

## Slide 26: Stacking or bonding? [Cu(CA)(1,10’-phen)]
IUCrJ, 2019, 6, 156-166.
Dalton Trans., 2014, 43, 7208-7218.

## Slide 27: Strong Interactions
Pancake bonding between planar radicals
Significant covalent component: multicentric two-electron covalent bonding
Electrostatic contribution
E > 15 kcal mol-1

## Slide 28: Pancake bonding between semiquinone radicals: KCl4Q·MeCOEt
200 K
Antiferromagnetic
3.27 Å
3.27 Å
3.58 Å
3.58 Å
3.46 Å
3.46 Å
3.46 Å
3.46 Å
Reversible!
Single crystal
to
Single crystal
CrystEngComm, 2012, 14, 7958-7964.
100 K
Diamagnetic

## Slide 29: Three types of pancake-bonded stacks: N-MePy·Cl4Q, [N-Me-4-(Me)2NPy]2(Cl4Q)3
A
B
IUCrJ, 2019, 6, 156-166.
Cryst. Growth Des., 2016, 16, 4777-4782.
Chem. Eur. J., 2018, 24, 8292-8297.
dimers
equidistant radicals
trimers
2.84 Å
3.59 Å
2.86 Å
3.60 Å
3.17 Å

## Slide 30: Interactions between the rings in a pancake-bonded dimer
Offset: 2.07 Å
0.5 e Å-3
2.86 Å
IUCrJ, 2019, 6, 156-166.
Cryst. Growth Des., 2019, 19, 391-402.

## Slide 31: Critical points in a pancake-bonded dimer
2.86 Å
3.60 Å
(3, -1) bond
(3, +1) ring centroid
(3, +3) cage centroid
ρmax > 0.095 e Å-3
ρmax < 0.040 e Å-3
IUCrJ, 2019, 6, 156-166.
Cryst. Growth Des., 2019, 19, 391-402.

## Slide 32: Pancake bonded dimer: HOMO orbitals
Intermolecular bond order | 
all atoms | 0.80
only C atoms | 0.27
inter-dimer | 0.04
Covalent contribution: –9.4 kcal mol-1
IUCrJ, 2019, 6, 156-166.
Cryst. Growth Des., 2019, 19, 391-402.

## Slide 33: Interactions between the equidistant radicals
Offset: 2.06 Å
0.5 e Å-3
3.17 Å
IUCrJ, 2019, 6, 156-166.
Cryst. Growth Des., 2019, 19, 391-402.

## Slide 34: Critical points between equidistant radicals
3.17 Å
(3, -1) bond
(3, +1) ring centroid
(3, +3) cage centroid
ρmax < 0.050 e Å-3
IUCrJ, 2019, 6, 156-166.
Cryst. Growth Des., 2019, 19, 391-402.

## Slide 35: Pancake bonding between equidistant rings: HOMO orbitals
Intermolecular bond order | 
all atoms | 0.26
only C atoms | 0.09
Covalent contribution: –2.9 kcal mol-1
IUCrJ, 2019, 6, 156-166.
Cryst. Growth Des., 2019, 19, 391-402.

## Slide 36: Pancake bonded polymer!
e-
e-
e-
e-
ΔE = 0.34 eV
IUCrJ, 2019, 6, 156-166.

## Slide 37
2–
1+
1+
Charges from Pval:
–0,76
–0,58
–0,58
–1.92
+0.96
+0.96
Pancake-bonded trimers in
[N-Me-4-(Me)2NPy]2(Cl4Q)3
IUCrJ, 2019, 6, 156-166.
Chem. Eur. J., 2018, 24, 8292-8297.

## Slide 38: Pancake bonding between three rings
2.84 Å
3.59 Å
ρmax > 0.077 e Å-3
ρmax < 0.045 e Å-3
IUCrJ, 2019, 6, 156-166.
Chem. Eur. J., 2018, 24, 8292-8297.

## Slide 39: Pancake bonding between three rings: HOMO orbitals
Intermolecular bond order | 
all atoms | < 0.71
probably | ~ 0.5
Covalent contribution: –4.11 kcal mol-1
IUCrJ, 2019, 6, 156-166.
Chem. Eur. J., 2018, 24, 8292-8297.

## Slide 40
Electric conductivity
Cl4Q∙N-MePy
Br4Q∙N-MePy
DDQ∙N-Me-2Pic
vs. interplanar distance (100 K)
3.2855(16) Å
3.1587(13) Å
3.122(3) Å
CrystEngComm, 2018, 20, 1862-1873.

## Slide 41
Inductive effect of the substituents
Cl4Q
Br4Q
DDQ
HOMO
HOMO
HOMO
LUMO
LUMO
LUMO
ΔE
ΔE
ΔE
CrystEngComm, 2018, 20, 1862-1873.

## Slide 42: New research: pancake bonding under extreme conditions
Collaboration with E. V. Boldyreva (Novosibirsk State University)
Variable-temperature crystallography (80 – 400 K)
High-pressure crystallography (up to ca. 10 GPa)
Electric conductivity and magnetism measurements under high pressure?

## Slide 43: Conclusions
 | weak | medium | strong
E / kcal mol-1 | < 5 | 5 - 15 | 15
Dominant interaction | dispersion | electrostatic | covalent
Hydrogen bonding | C-H···O, C-H···S, C-H···Cl | O-H···O, N-H···N, O-H···N | RAHB, CAHB, LBHB, HF···FH, OH2···H+···H2O (Zundel ion)
Halogen bonding | C-Cl···O | N-Br···N, N-I···N | N-bs···3,5-dmp, halonium ions
π-stacking | aromatics, heteroaromatics... | quinones, metal-chelates | planar radicals: dimers, trimers, equidistant stacks
IUCrJ, 2019, 6, 156-166.

## Slide 44: Acknowlegdements
Croatian Science Foundation, grant no. IP-2014-09-4079
Croatian Academy of Sciences and Arts
French-Croatian bilateral, Slovenian-Croatian bilateral
RBI, Zagreb
Biserka Kojić-Prodić
Zoran Štefanić
Marijana Jurić
Lidija Androš Dubraja
Nadica Maltar-Strmečki
Ana Šantić
Dijana Žilić
Darko Babić
Valentina Milašinović
Lidija Kanižaj
Université de Lorraine
Christian Jelsch
Claude Lecomte
Emmanuel Wenger
Slimane Dahaoui
University of Zagreb
Vladimir Stilinović
Damir Pajić
Nikolina Novosel
Krešo Zadro
University of Ljubljana
Anton Meden
KI, Ljubljana
Jernej Stare
Gregor Mali
Dušan Hadži
Jože Grdadolnik
Rigaku Oxford Diffraction Ltd.
Marcus Winter
Dyanne Cruikshank
Georgetown Univ., USA
Miklosz Kertesz
Zhongyu Mou
UNAM, Mexico City
Jesús Hernández-Trujillo
Bruno Landeros-Rivera