Possible signatures of ferroelectricity in antiferromagnetically ordered zig-zag spin chain

M. Dragičević1, Ž. Rapljenović1, D. Rivas Góngora1, T. Ivek1, M. Pregelj2,

A. Zorko2, H. Berger3, D. Arčon2,4

1Institute of Physics, Bijenička cesta 46, HR-10000 Zagreb, Croatia

2Jožef Stefan Institute, Jamova c. 39, 1000 Ljubljana, Slovenia

3Ecole polytechnique fédérale de Lausanne, CH-1015 Lausanne, Switzerland

4Faculty of Mathematics and Physics, University of Ljubljana, Jadranska c. 19, 1000 Ljubljana, Slovenia

e-mail: mdragicevic@ifs.hr

Unconventional orderings of spin may provide a way to form multiferroic phases. For instance, spiral magnetic orders can break the space inversion symmetry and create electric dipoles which is a prerequisite for ferroelectric ordering [1]. One such candidate system is the zig-zag spin chain β-TeVO4 which has a complex magnetic phase diagram at low temperatures.  From the paramagnetic high-temperature phase, the system enters the antiferromagnetic incommensurate spin-density wave phase at TN1=4.65 K. Then, at TN2=3.28 K it forms the so-called spin stripes which establish as a second incommensurate spin-density wave is superimposed on top of the first one. Finally, the difference between their two wave vectors disappears at TN3=2.26 K and the system enters its ground state – the vector chiral phase. Interestingly, at this last phase transition the electric dipoles become allowed by crystal symmetry. [2,3,4]

In this work we investigate the possibility of ferroelectricity in the spin-ordered phases of β-TeVO4 using dielectric spectroscopy and static polarization measurements in the presence of external magnetic field. We discuss the obtained nonlinear dielectric properties in the context of its magnetic phase diagram.

[1] K. F. Wang, J. M. Liu, and Z. F. Ren, Adv. Phys 58, (2009), 321–448

[2] M. Pregelj, A. Zorko, O. Zaharko, H. Nojiri, H. Berger, L. C. Chapon, and D. Arcon, Nature Communications 6 (2015),  10.1038/ncomms8255.

[3] M. Pregelj, O. Zaharko, M. Herak, M. Gomilsek, A. Zorko, L. C. Chapon, F. Bourdarot, H. Berger, and D. Arcon, Phys. Rev. B 94, 081114 (2016).

[4] M. Pregelj, A. Zorko, M Gomišlek, M. Klanjšek, O. Zaharko, J. S White, H. Luetkens, F. Coomer, T. Ivek, D. Rivas-Góngora, H. Berger, D. Arčon, npj Quantum Materials 4, 22 (2019)