BIOCOMPATIBLE MEMBRANES - A CONTROVERSY DESERVING

ATTENTION

Vladimir Gašparović MD1, PhD, Kristina Đaković MD2, Hrvoje Gašparović MD2, Marijan Merkler MD1, Radovan Radonić MD1,  Dragutin Ivanović MD1, Josip HusarMD3, Ivan Jelić MD, PhD3

1Department of Emergency and Intensive Care Medicine, Department of Internal medicine, Rebro, Zagreb, Croatia

2Medical School, University of Zagreb, Croatia

3Department of Surgery, Rebro, Zagreb, Croatia

key words: biocompatible membranes, acute renal failure, outcome

Abstract: The persistently high mortality rate of patients with acute renal failure (ARF) calls for intensive exploration of different modes of management. The institution of biocompatible membranes into the treatment of ARF resulted in controversial opinions regarding its benefit. Our study showed that the outcome of patients in whom ARF followed a surgical procedure was better in the group which underwent hemodialysis on the polysulfone membrane (BC group) when compared to the group in which the modified cellulose acetate membrane (BIC group) was used (p=0,0223 Chi square test). We have also found that the renal function in the BC group  recover sooner, requiring a fewer number of extracorporeal circulation sessions.  It is important to stress that the BC and BIC group included patients of comparable severity of the underlying disease as is documented by the mean APACHE II scores of each group.

INTRODUCTION:  Various endeavors to improve the outcome of patients with ARF have not proven to be efficient (1,2,3). Few issues have brought on as much disagreement as did the introduction of biocompatible membranes into the management of the clinical syndrome of ARF. The results were controversial and inconclusive (4,5,6,7,8). The mentioned procedure is more costly, therefore necessitating that its benefit be carefully assessed. The aim of our study was to evaluate the results of hemodialysis treatment of patients with ARF on the polysulfone membrane (BC) in comparison to the standard regimen in which the modified cellulose acetate membrane is used (BIC).

PATIENTS AND METHODS: Our investigation of the role of the biocompatible membrane in comparison to the standard modified cellulose acetate membrane was founded upon our results in the last year. A group of 49 patients scheduled for hemodialysis which included both surgical and medical patients, consisting of 34 males and 15 females,  mean age  61,73+/-12,99 years, was the basis of our analysis. The above mentioned group of patients was subdivided into two groups with respect to the membrane which was used in the hemodialysis protocol (group BC (24 patients): polysulfone membrane; group BIC (23 patients): modified cellulose acetate membrane).

Acute renal failure was defined by azotemia (serum creatinine >400 mol/L) with or without oliguria, and by serum potassium levels exceeding 5,5 mmol/L. The dialysis blood flow was 150-200 mL/min, and the dialysate flow was 500 mL/min. The duration of a single hemodialysis session was 3-3,5 hours. There was a minimum of 6 dialysis sessions a week. The levels of serum creatinine, urea, sodium and potassium were observed and documented prior to as well as following hemodialysis. Certain other biochemical parameters were also noted. Two of our patients (Number 4 and Number 35) were excluded from the study either because the data gathered was insufficient to meet the standards of this study or due to a different type of hemodialysis membrane. Patients on either membrane were dialyzed without heparin. The biocompatible polysulfone membrane used was the Fresenius F60 membrane, whereas our modified cellulose acetate membrane was the MCA 130 with an area of 1,3 m2. APACHE II Scores were noted at the introduction into the study and 1,2,3,7,14 and 21 days after the commencement of hemodialysis and thus labeled APACHE II 0,1,2,3,7,14,21. We have separately analyzed the outcome of patients suffering from multiple organ failure (at least two organ systems insufficient, one of which is the renal system) with respect to the type of membrane used in their hemodialysis protocols. Our statistical analysis included the t-test for independent samples for the APACHE II Scores, the 2 test and the Fisher test for the patient outcome with regard to the two types of membranes.

RESULTS: The difference in the outcome of patients with ARF with respect to different membranes used for hemodialysis may be seen in Table 1.

Table 1.

The most frequently observed disorders leading to the development of ARF

| GROUP | DIAGNOSIS | APACHE II0 | APACHE II1 | APACHE II7 | OUTCOME |
| --- | --- | --- | --- | --- | --- |
| GROUP 1 BIC | 1(14),2(3),3(3)4(2),7(1) | 34.65+/-11.22 | 32.77+/-11.86 | 27.23+/-10.7 | 5*/23 |
| GROUP 2 BC | 1(16)2(4)3(1) 4(1),5(1),6(1) | 31.04+/-9.5 | 29.54+/-9.76 | 29.12+/-11.92 | 13*/24 |
| p |  | ns | ns | ns | 0.0223** 0.0355*** |

*survivors

**Chi squre test

***Fisher exact two tailed test

DIAGNOSIS

1=sepsis following open heart surgery

2=sepsis following abdominal surgery

3=vasculitis

4=sepsis in the medical ICU

5=leptospirosis

6=rabdhomiolysis

7=severe heart failure

The mean number of haemodialysis required for recovery of renal function in surviving patients with ARF is presented in Table2.

Table 2.

AVERIGE  NUMBER OF HAEMODIALYSIS PROCEDURES REQUIRED FOR RENAL RECOVERY IN SURVIVORS WITH ARF

|  | SURVIVORS | AVERIGE NUMBER OF HD+/- SD UNTIL RENAL RECOVERY |
| --- | --- | --- |
| GROUP 1 | 5 | 21.2+/-10.42 |
| GROUP 2 | 13 | 9,85+/-8,92 |
| p | 0.048316 Chi square |  |
|  | 0.019788 Mann Whitney test. |  |

The difference in the outcome of patients with ARF and respiratory insufficiency requiring  artificial ventilation  with respect to different membranes used for hemodialysis may be seen in Table 3.

Table 3.

THE OUTCOME OF PATIENTS WITH MOF DEPENDANT  OF THE TYPE OF HEMODIALYSIS MEMBRANE USED

|  | SURVIVED | SURVIVED+RESPIRATOR** | DIED | DIED+RESPIRATOR** | TOTAL ALIVED | TOTAL DIED |
| --- | --- | --- | --- | --- | --- | --- |
| BIC | 3 | 2 | 3 | 13 | 5 | 16 |
| BC | 7 | 6 | 1 | 10 | 13* | 11 |
| TOTAL | 10 | 8 | 5 | 23 | 18 | 27 |

*McNemar Chi square p=0.0265

** Patients with ARF & respiratory failure requiring artificial ventilation

GROUP 1 = MODIFIED CELLULOSE ACETATE MEMBRANE

GROUP 2 = POLYSULPHONE MEMBRANE

DISCUSSION: Certain studies have established the incidence of ARF in hospital patients at approximately 5%. The incidence of ARF development in ICU patients, however, is approximately 30%. Many procedures have been undertaken in improving the outcome of the affected patients (9,10). The high mortality rates can be explained by the occurrence of ARF in the clinical syndrome of multiple organ failure (MOF), where the underlying disorder determines the prognosis. The resistance to treatment of the basic process resulting in MOF cripples the efforts for organ function restitution. This should be an encouragement for the development of new techniques, which could reduce the mortality rates of patients with ARF. Though biocompatible membranes have offered contradictory results, certain reports of their benefit should stimulate a prospective study of this problem.

more aggressive types of treatment often recently employed result in an increase in ARF frequency. Inclusion of the elderly population into the more aggressive medical management, wars and trauma, as well as radical approaches in cardiac and abdominal surgery, maintain the mortality rates of patients with ARF between 60 and 70% (11,12). Our goal was to determine the variance in the outcome of patients with ARF when different types of hemodialysis membranes were used. The severity of the underlying condition upon inclusion into the study was not different in the two groups we observed, accordin APACHE II score (13). Recognizing the fact that the APACHE II score was somewhat higher in a group 2 (the difference was not statistically significant) we have separately analyzed patients with ARF following sepsis, in an effort to evaluate the accuracy of the results. The severity of the disease was comparable in both groups. It is important to note that the survival rates of the patients with ARF were higher in the group of patients who were subjected to hemodialysis on the biocompatible polysulfone membranes, when compared to the patients dialyzed on the modified cellulose acetate membrane. Patients developing ARF secondary to sepsis following open heart and abdominal surgery, as well as those suffering from ARF caused by medical sepsis, were studied apart from the patients developing ARF as a result of a non-septic etiologic factor. The group of patients with ARF secondary to sepsis dialyzed on biocompatible membranes recovered sooner with a significantly lower number of hemodialysis sessions required for the renal function recovery (14). Furthermore, in the patients suffering from ARF in whom the condition was further aggravated by an acute respiratory insufficiency warranting the use of artificial ventilation we have demonstrated a better outcome when the biocompatible membrane was used in hemodialysis. We believe that these results deserve a detailed investigation. As we have already emphasized the severity of the basic disorder leading to MOF is of paramount importance. This may explain why the amount of produced urine did not present a prognostic factor in our patients. The occurrence of diuresis in a previously anuric patient did not affect the final outcome. If the septic process remained out of control the evolution of kidney function recovery could not prevent a lethal outcome. That is to say that the importance of control over the underlying condition could not be overemphasized (15).

The mortality rate of ARF remains high. Patients die in the clinical syndrome of MOF, despite the utilization of artificial ventilation, vasoactive therapy and hemodialysis. The high mortality rates of patients dialyzed on both the biocompatible and the bioincompatible membrane is secondary to protracted sepsis caused by resistant micro-organisms which usually progresses to death.

We also believe that the institution of biocompatible membranes into the treatment of patients with ARF has improved their chances for a favorable outcome (16). The use of biocompatible polysulfone membrane in acute renal failure, along with other measures, represents an advancement in patient management. Our data justifies a randomized study because we believe  that the results presented in this article are encouraging and that they offer new hope in the treatment of patients with ARF.

Literature:

1. 	Alkhunaizi AM, Schrier RW. Management of acute renal failure: New perspectives, Am j.Kidney Dis, 28:325-328, l996.

2. Gubern JM,  Sancho JJ,  Simo J,  Sitges-Serra R.R. Randomized trial on the effect of mannitol on

postoperative renal function in patients with obstructive jaundice. Surgery, 103:39-44, 1988.

3. 	Bonomini V, Coli L, Maria Scolari, Stefoni S. Structure of Dialysis Membranes and Long-Term Clinical Outcome. Am J Nephrol 15:455-462, 1995.

4. 	Schiffl H,  Lang SM,  Koenig A, Strasser T, Haider MC, Held E.. Biocompatible membranes in acute

renal failure: prospective case-controlled study. Lancet 344:570-2. 1994.

5.   Hakim RM, Wingard RL, Parker RA: Effect of the dialysis membrane in the treatment of patients with

acute renal failure. N Engl J Med, 17, 1338-1341, 1994.

6.  Shaldon S. Biocompatible membranes in acute renal failure. Lancet, 347:205, 1996.

7. 	Kurtal H D von Herrath, Schaefer K: Is the Choice of Membrane Important for Patients with Acute Renal Failure Requiring Hemodialysis. Art Org, Boston, Vol 19, No.5 391-394, 1995.

8. 	Kaplan A, Paganini P, Bosch P. Effect of the dialysis membrane in acute renal failure. N Engl. J

Med. 332:961-962,1995.

9. 	Corwin HL,  Bonventre JV. Acute renal failure in the intensive care unit. Part 2. Intensive Care Med

14:86-96,1988.

10. 	Turney JH. Acute renal failure-some progress?, N Eng J Med, 331:1372-1374,1994

11. 	Lameire N, Matthys E, Vanholder R, De Keyser K, Pauwels W, Nachtergaele H, Lambrecht L,  Ringoir S. Cause  and prognosis of acute renal failure in elderly patients. Nephrol Dial Transplant 2:316-322, 1987.

12. Gašparović V, Radonić R, Gjurašin M,  Gašparović H, Ivanović D, Merkler M,  Jelić I. Aetiology

and outcome of acute renal failure secondary to war related trauma and infectious disease in Croatia.

Nephrology, 3:155-158, l997.

13. 	Knaus WA,  Draper EA, Wagner DP,  Zimmerman JE. APACHE II. a severity of disease

classification system. Crit Care Med 13:818-829,1985.

14. 	Gašparović V, Djaković K, Gašparović H, Merkler M, Ivanović D, Pišl Z, Majerović M, Jelić I. Biocompatible membranes in acute renal failure (ARF), hope or illusion?, Nefrologia, 18:27-31, 1998.

15. 	Jacobs C. Membrane biocompatibility in the treatment of acute renal failure:what is the evidence in

1996 ?, Nephrol Dialys Transpl, 12:38-42,1997

16. 	Himmelfarb J. Tolkoff Rubin Nina, Chandran P,  Parker RA, Rebecca L Wingard, Hakim R. A

Multicenter Comparison of Dialysis Membranes in the Treatment of Acute Renal Failure Requiring

Dialysis. J Am Soc. Nephrol 9:257-266, 1998.