# Introduction

Intensive development of a Finite Element FE programs brings them close to the application and everyday engineering praxis. After (Mackerle, 2002) in the year 2002 there have been 1538 FE programs registered. The major commercially available FE programs for forming process simulation are enumerated in (Haepp & Roll 1999). Their availability enabled the production engineers to use them for obtaining the quick answers to a non typical problems emerging in everyday engineering praxis (Soltani et al., 1997) or (Altan et al. 1995).

Commercial FE programs can be used in parallel with the experiment while researching a bulk metal forming technology. The result is improvement of both, FE and experiment. Likewise obtained FE model can be used for giving mentoned quick answers for similar processes. In estimation of those similarities only the experienced engineers can take a serious part by having an insight in both; principles of FE analysis and real metalforming process. Therefore to enable a simultaneous engagement in applied FEM and praxis there was a need to give a brief review of the used Finite Element Method and it was done in this paper.

All the steps from the principle of the virtual work to the iterative solvers used in Marc are explained in order to clarify the main problems in structural, non linear analysis. Since MSC Marc is a universal solver used as a module in many different CAM software, this paper should provide an insight in Marc FEM solution techniques. In the end, a bulk metal forming process – radial gear extrusion of a gear is performed to demonstrate a capability of the used software.

# Review of the used FE method

  - From the principle of the virtual work to the stiffness equation

The main goal of building an FE analysis is to obtain the unknown fields u that are expressed in terms of the nodal point unknowns v by the use of shape functions N. Those fields can be defined using material or spatial coordinates. Mathematically speaking both approaches give the same result, but Lagrangian frame of reference using material coordinates is chosen. It is done since in the radial gear extrusion a contol surface of a billet becoming a gear is a non stationary surface and therefore more easily described using the material coordinates attached to the initial billet geometry. Moving together with the material, material coordinates are also more adequate for modeling a strain hardening. Written for a single element e, using the current stete as a reference state, a principle of the virtual work can be transformed into the following equation;

|  | (1) |
| --- | --- |

where Bimn is the symmetric gradient operator evaluated in current configuration, Lmnpq is the material moduli tensor in current configuration, eand e are the single element volume and surface respectively, Ni is the shape function, N is the shape function matrix, vje are the unknown element nodal displacements, f e  is the element body force vector, t e is the element traction force vector and F is the sum of concentrated nodal forces acting upon single element.

Equation (1) represents a stiffness equation of a single element e. It can be rewritten in short form as the element stiffness equation Ke v e =  – f e. In order to equilibrate the whole geometry divided into the finite element mesh, single element stiffness equations have to be assembled over the whole model geometry. Thus we obtain a global stiffness equation:

|  | (2) |
| --- | --- |

Where K is the stiffness matrix K = Ke,  f  is the nodal load vector f  = f e and v is the nodal displacement vector v = T -1 v e. T is the orthogonal transformation matrix. In order to solve the global stiffness equation (2) it is necessary to define the boundary conditions. The result of setting up the boundary conditions is a partitioning of the nodal displacement vector, that implies a partitioning of the stiffness equation as shown in (3).

|  | (3) |
| --- | --- |

Where vu are the unknown nodal displacements and vs are the specified nodal values, fa are the applied nodal loads and fr are the nodal point reactions.

System of equations (3) is a nonlinear system because in the bulk metal forming simulation, there are three sources of nonlinearity. First is the material nonlinearity coming from the strain hardening that numerically influences the material moduli tensor in equation (1). Second is the problem of the geometrical nonlinearities influencing the second term on the left hand side of the equation (1). Both, material and geometrical nonlinearity influences the stiffness matrix in (2). Finally, third source of nonlinearity is a friction model that, dependent on actual state, influences the global load vector.

In order to simplify the numerical models in this paper, the friction as a third source of nonlinearity was left out. Having two sources of nonlinearity included in our FE model, nonlinear system of equations (4) has to be solved using an iterative approach, briefly described by the scheme shown in Fig. 1. Every increment is subdivided into the subincrements known as cycles. Each cycle contains three major numerical steps; assembly, solve and recover, each consuming the same amount of the CPU time, while in linear analysis steps of assembly and recover are significantly shorter. Used algorithms for each one of the mentioned steps, greatly differ from one solver to the other and for this reason it is correct to consider the FE method as a technology.

Fig. 1. Iterative solution flow diagram performed by MSC Marc solver.

Assembly of the global stiffness matrix is performed at each beginning of the cycle. After the assembly, nonlinear system of equations is solved using Newton – Raphson method. Cycles including assembly of the stiffness matrix, solving and recovery are repeated until the convergence criterion has not been satisfied. After the nodal displacement field has been obtained program calculates the nodal load vector and consequently pursues a relative residual force check as a criterion of proceeding to the next increment. Number of recycles over the increments for performed simulation of bulk metal forming is given in Fig. 6.a Brief overview of relative residual force check is given in equation (4).

|  | (4) |
| --- | --- |

Freaction in enumerator represents a difference between the external and internal forces at each node for the degree of freedom with a largest magnitude. fr in denominator represents a maximal reaction force at a different degree of freedom with a largest magnitude. Most commonly it is required for the Freaction to be ten times smaller than the fr (Tol = 0.1). Besides the residual force check there is another parallel check, traditionally performed by the Marc solver. It consists in calculating the stiffness matrix singularity ratio R = C -1 where C is the mathematically well defined conditioning number of a matrix. If the problem is numerically well defined, after (MARC Primer introductory textbook, 1993) and (MSC Marc theory and user information, 2003), the values of R should remain between 100 and 10-4.

Figure 6.b shows that in both simulations performed, singularity ratio criterion has been satisfied during all the increments, and the simulations can be considered as a well defined structural analysis problem. Precise definition of the stiffness matrix singularity ratio R can be found in (MSC Marc theory and user information, 2003).

After the determination of the nodal displacement vector v MSC Marc solver recovers the unknown displacement, stress and strain fields by substituting the element nodal displacements v e=T v into the following equations;

| uev e | (5) |
| --- | --- |
| ev e | (6) |
| eL e | (7) |

Where ueare the displacements inside the particular element, e are the strains and e are the stresses inside a particular element,  and L are the shape function, gradient operator and material moduli tensor respectively. It is interesting to point out that in the Updated Lagrangian approach a compatibility of the displacement fields along the mutual border of two adjacent elements, does not imply a compatibility of the stress field along that border. This problem is diminished when using a finer FE mesh.

# FE SIMULATION

3.1 Preprocessing - creation of the geometry for the structural analysis

Before the numerical crunching performed by the solver takes place, all the data relevant for the FE analysis has to be prepared by the use of the program called preprocessor. In this paper MSC.Mentat preprocessor has been used since it was developed in parallel with the MSC Marc solver and therefore gives the opportunity of 100% use of the MSC Marc capabilities. There is also an option of using MSC.Patran as the preprocessor with a slight smaller use of the mentioned capabilities.

One of the first steps in creating a geometry and a mesh for the structural analysis is a creation of the geometry. In the considered simulation first step is turning the tool and workpiece geometry into numerical objects. Regarding surfaces, this operation was done using NURBS, a Non Uniformal Rationl B Splines that smoothly model simple surfaces shown on the Fig. 2. In the case of the surfaces with a lot of complex details one should use a picewise linear representation instead of analytical NURBS approach. This simplifies the complex procedure of determining a contact status that is very important to the stability of FEM model, as it will be shown in post processing of the results. If using other CAD program for creation of the geometry there is a need to check whether used preprocessor is or is not capable of reading the particular format. The orientation of the surfaces in preprocessor is of great importance and badly defined surfaces can sometimes preclude the simulation to be performed.

Fig. 2. a) Numerical modelling of the rigid contact bodies included in linear elements analysis. b) Meshed deformable body enclosed by the rigid bodies

Fig. 3. a) Numerical modeling of the rigid contact bodies included in parabolic element analysis. b) Meshed deformable body with boundary conditions set upon the nodes.

Second step is the creation of FE mesh when the desired bodies are subdivided into the finite elements. This meshing operation can be performed on all geometries included in structural analysis, but in most cases only the body of interest is converted to the FE mesh and other bodies are considered as rigid ones Fig. 2 and Fig. 3. It is done so to reduce the overall number of FE included in simulation. In performed simulation only the Al billet, that will become a gear of the specified geometry, is subdivided into the FE mesh Fig. 2.b and Fig. 3.b, while the punch, lower plate and the outer planes are considered as rigid bodies Fig. 2.a and Fig. 3.a. (Hatangady, 1999) has introduced an interesting algorithm for meshing of the rigid bodies with a minimum number of FE elements necessary for correct representation of adjacent stress fields.

After all the object and element geometries have been created a particular element type has to be assigned to the FE mesh. For the structural 3D analysis MSC Marc offers 2 groups of element types; with a linear shape function N and with the parabolic shape function N. This is also known as division onto the low order – linear elements and high order – parabolic elements. For the purpose of this analysis two elements were used; a linear element type 134 with four nodes and a parabolic element type 127 with ten nodes, both shown in Fig. 4 and precisely described in (MSC Marc Element library, 2003).

Since the gear geometry is axisymmetric, simulation was performed over one sixth for the element type 127 and over one twelfth for the element 157. The reason of making this difference is the requirement and restriction of Marc solver concerning the use of a different element types and remeshing.

For the equation (3) to become a partitioned system of equations (4) in the process of assembly, there is a need to set up a boundary conditions upon the created model. If this operation of restraining of global degrees of freedom is performed correctly, a global stiffness matrix becomes a positive definite, having good properties for the numerical analysis. Other warranty of having a good conditioned problem is a fact that the stiffness matrix singularity ratio R for both simulations remains between 1 and 10-4 for every increment during the simulation as shown in Fig. 6.b.

Fig. 4. Simple, visual representation of the a) linear, four noded element b) parabolic, ten noded element

In the linear elements model, boundary conditions were set up using the wedge axisymmetric planes as shown in Fig. 2.a. Those planes restrain the degrees of freedom of all the nodes lying along those planes that cut off one twelfth of a billet. In the parabolic element model, the boundary conditions were set up using the nodal boundary conditions set upon the nodes as shown in Fig. 3.b. The formulation of boundary conditions using wedge planes is more general and allows the necessary remeshing of linear element mesh. In comparison to the parabolic, linear elements are about three times more sensitive to the distortion of the FE mesh.

Material properties have been assigned to the FE model and material was modeled as a rigid plastic Al material with strain hardening curve taken from the flowchart (VDI 5-3200, 1954).

3.2 Numerical crunching

Numerical crunching performed by the MSC Marc solver took about 90 hours for the parbolic 10000 elements model and 3 hours for linear 14000 elements model on 1.8 GHz Windows 2000 OS. The difference in solution time comes from the use of different element types, pointing out at the linear elements as a faster solution for simulating the finite strain. Nevertheless, parabolic elements keep their quality in better withstanding of the large deformations, enabling the whole simulation to be performed without remeshing! This quality makes parabolic element simulation more similar to the real metalforming process. Therefore it would be advisable to widen the software for large deformations with the improved algorithms for parabolic element models.

3.3 Postprocessing

Once the used solver MSC Marc has finished a numerical crunching of the input data, and all the required element tensors, element scalars and nodal quantities have been calculated, postprocessing takes place. It can be done using any software capable of reading the MSC Marc binary results *.t16 file. In performed simulation MSC.Mentat was used also as postprocessor for its greatest compatibility with MSC Marc solver.

Fig. 5. Force stroke diagram obtained in each one of the two performed simulations

The main FE analysis result is the force – stroke diagram shown in Fig. 5. The final steep load rise belonging to the final stage of corner filling has a 0.52 mm delay on parabolic element simulation since it is performed without remeshing and a distortion of the FE mesh is severe with a 1.25% overall element volume loss, implying a larger stroke needed to fill the gear cavity.

Linear elements model

Fig. 6. a) Number of cycles performed inside every increment, helping to indicate numerically problematic situations during the FE simulations. b) Evolution of the stiffness matrix singularity ratio over the increments

Looking at the force – stroke diagram in Fig. 5, there is one stair at the very beginning of the simulation coming from a fact that there is no initial nodal load and displacement vector to base the iteration upon. Secondly there is a remeshing included in simulation using general formulation of the boundary conditions via axisymmetric planes that are numerically much more difficult to handle. Mentioned two facts resulted in a large number of recycles in the beginning of the simulation, necessary to obtain the equilibrium, Fig. 6.a. Second force jump on the force – stroke diagram and recycle – increment diagram appears in increments 46 and 47 as a clear sign that a deformed FE billet came in contact with the outer planes surface inside a gear cavity as shown in Fig. 7.a.

Large force jump at increment 57 belongs to the action of remeshing when entirely new mesh with a new interpolated nodal positions have brought the largest numerical deviation to the nonlinear system of equations (3). Therefore it is recommended to find a criterion that results in minimal number of remeshes. Second remeshing at the increment 79 brings also a force jump but to the much smaller extent. Two mentioned remeshes were necessary and sufficient to simulate a good gear cavity fulfillment as it can be seen in Fig. 8 and Fig. 7.b. All the other small force jumps visible in the force – stroke diagram are coming from the change of contact status influencing a nodal displacement vector v and nodal load vector f  in the stiffness equation (2).

Parabolic elements model

In the beginning of the force – stroke diagram there is also a force jump coming from a sudden loading in the FE model. Since the boundary conditions were set upon the nodes, equilibrium is reached in less cycles than in the linear elements model. During the increment 18, FE billet reaches the outer planes and the change of the contact status requires a larger number cycles for reaching the equilibrium by satisfying residual force convergence criterion. This change of the contact status, alters the nodal displacement vector v in equation (2) by increasing the number of unknowns and consequently a number of necessary cycles over the following increments.

Fig. 7. a) An arrow showing the beginning of a contact inside the gear cavity, realized between the FE deformable body and outer planes as rigid bodies. b) A final stage, linear elements model.

Greater number of 15000 nodes over 10000 elements and a parabolic shape function resulted in 90 hour simulation while linear elements simulation with 12 000 nodes over 55000 elements MSC Marc performs in 3 hours. Such a difference in calculation time can be attributed to the fact that parabolic elements have four integration points, for representation of the unknown fields, while the linear element type used has only one integration point.

# Conclusion

Fig. 8 Equivalent plastic strain visualised by the use of the contour bands. a) side view shows a good gear cavity corner fulfillment b) different view of the same strain distribution.

Although both FE models represent a numerically well explainable simulation of the bulk metal forming of a gear, the difference in obtained force – stroke diagrams, regarding the work done is 20%. This large difference between the numerically obtained results implies a need of analytical and experimental approach as authors performed in (Choi & Choi, 1997).

When used, numerics should be considered as a technology due to the large number of modelling possibilities regarding FE method and Preprocessing. More precise and necessary criterion for estimating the value of the performed simulations would be in their comparison with the experiment (Skunca et al. 2003). Those comparison can be done via experimentally recorded force stroke diagram as performed in (Plancak et al., 2003) or via the experimentally measured microhardness that can be compared with the simulated equivalent strain as authors performed in (César et al., 1997) . The best approach is to compare the FE simulation and experiment using both mentioned criteria.

Since iterations are present in all the finite strain numerical simulations, it is advisable, in presence of experiment or not, to perform the numerical checks, similar to the ones used in this paper. Accordance of the numerical checks with the characteristical events in simulated technology, i.e. realization of the contact inside a gear cavity, is the additional warranty of having a good FE simulation. Besides, numerical checks are the only way of avoiding the use of the commercially available FE programs like a black boxes, while the opportunity of discussion between the dedicated FE analyst and FE user in the workshop remains possible.

5. References

Altan T., Sweeney K., Vazquez V., Hyunkee. K & Knoerr M. (1995), Cold Forging of Complex Shaped Parts to Close Tolerances-Application of Metal Flow Simulation to Process and Tool Design, Proceedings of the 9th Inernational Forging Congress, Solihull UK, pp. 168-177, ISBN 0-86108-956-1

César de Sá J., Martins P. A. F., Peterson S. B., Rodrigues J. M. C., Costa Sousa L. & Madureira M. L. (1997). Simulation and optimisation of radial extrusion of components by virtual prototyping, Proceedings of NAFEMS world congress '97, ISBN 1 874376 20 4, pp. 359-382, Stuttgart, Germany, April 1997, NAFEMS Ltd Scottish Enterprise Technology Park Glasgow.

Choi J. C., Choi Y. (1997). A study on the forging of external spur gears: upper-bound analyses and experiments. International Journal of Machine Tools & Manufacture 38

Haepp, H. J. & Roll K. (1999). Future perspectives and limits for the mathematical modelling of metal forming processes in automotive industry, Proceedings of the 6th international Conference on Technology of Plasticity, Geiger, M. (Ed.), pp. 481-488, ISBN 3-540-66066-6, Nuremberg, September 1999, Springer-Verlag, Berlin Heidelberg New York Tokio

Mackerle, J. (2002), FEM and BEM in the context of information retrieval, Available from: http://www.solid.ikp.liu.se/fe/JM1/Prednaska.PPT Acessed: 2004-02-23

MARC Analysis Research Corporation (1993), Primer introductory textbook, MARC Analysis Research Corporation, 260 Sheridan Avenue,  Palo Alto, CA 94306, USA

MSC.Software corporation (2003), Element library, MSC.Software corporation, MacArthur Place, Santa Ana, CA 92707, USA

MSC.Software corporation (2003), Theory and user information, MSC.Software corporation, MacArthur Place, Santa Ana, CA 92707, USA

Plancak, M.; Skunca, M. & Math M. (2003). Numerical simulation of radial gear extrusion in cold state. Proceedings of CIM 2003 Computer Integrated Manufacturing and High Speed Machining, Cebalo, R. & Schulz, H. (Ed.), pp. IV073-IV083, ISBN 953-97181-5-5, Lumbarda, June 2003, Croatian Association of Production Engineering, Zagreb

Plancak M., Skunca M. & Math M. (2003). Analysis, FEM simulation and experimental verification of gear cold extrusion. Proceedings of the VIIth International Conference on Forging – XXIII SENAFOR, Schaeffer L. (Ed.), 28-39, ISBN ?, Porto Alegre - Brasil, Oct. 2003, Grafica e Editora Brasul Ltda - Porto Alegre/RS

Soltani B., Matisson K. & Samuelsson A. (2003). Implicit solid, flow and flow-solid finite element approaches in bvlade forging simulation. Int. J. Numer. Meth. Engng. 2003; 56:1861-1882 (DOI: 10.1002/nme.628)

Skunca, M.; Keran, Z. & Math M. (2003). Finite element modelling of radial gear extrusion, Annals of DAAAM for 2003 & Proceedings of the 14th International DAAAM Symposium, ISBN 3-901509-34-8, ISSN 1726-9679, pp 427-428, Editor B. Katalinic, Published by DAAAM International, Vienna, Austria 2003.