Axial vs angular dynamization of anterior cervical fusion implants: A prospective cohort study

Authors: Marin Stančić, Bojan Gluhačić, Tihomir Banić, Milan Milošević, Božo Radić and Gojko Buljat

# Division of Neurotraumatology, Clinical Hospital for Traumatology Zagreb,

# School of Medicine  University of Zagreb, and University of Rijeka, Croatia

## Abstract

Aim. To compare anterior cervical fusion with fusion augmented with dynamic implants and augmented with 1st generation “H”-plate.

Methods.  Patients with radiculopathy and/or myelopathy were included in a prospective cohort study. Clinical outcome was assessed according Nurick, Odom, and SF 36 scales. Rotation and translation of screws, and quality of fusion (Tribus) at 6-week and 2-year follow-up examination were assessed.

Results. In 56 patients neurodecompression (one-level N=30, two-level N=16 and multi-level N=10 ) was performed between January 2001, and September 2003. Thirtyfour male and 22 female patients were divided in 3 groups, depending on type of fusion: 1. Augmented with dynamic implants (N=23), 2. Augmented with “H”-plate (N=23), and 3. Non-augmented (N=10, one-level. There were no significant differences in clinical outcome between groups. Dynamization was detected in both augmented groups: axial in Dynamic implants group (mean translation ( SD = 2.67mm ± 0.79 mm), and angular in “H”-plate group (angle of rotation 7.2° ±  3.04°). Six-week fusion was significantly better in Dynamic implants and Non-augmented groups, comparing with “H”-plate group. Two patients in “H”plate group had pseudoarthrosis, 7 patients in Dynamic implants group had suprajacent segment heterotopic ossification with ankylosis in 2 patients. Three patients in Non-augmented group had dislogement of the bone graft with transient dysphagia in one of them.

Conclusion. Our results sugest that selection of implants are not crucial for clinical outcome. Subsidence is allowed with both fixation systems. Fusion is faster and more effective in the axially dynamized groupe.

Key words: surgical procedure, anterior, cervical plate, myelopathy , decompression, cervical fusion

###### Introduction

Cervical spondylotic myelopathy  is the most common pathological condition affecting the spine of the older persons (1, 2). Untreated CSM has progressive clinical course that could lead to a spastic paraplegia in elderity (3). The best type of surgical procedure for cervical radiculomyelopathy is not known (4). Decompression of the cord or the nerve root is the principal aim (5). Anterior cervical decompression was introdused in mid-1950s (6, 7). Although new surgical technique, following it’s first publication was criticaly compared with “russian tonsilectomy” it became widely accepted (8). Anterior cervical decompression is traditionally combined with fusion of the decompressed segment, although existing evidences show this may not be necessary or appropriate (9- 12).  Autologous bone graft with osteogenic, osteoconductive and osteoinductive properties, theoretically secure the best possible fusion what clinical practice has already confirmed (13, 14). High incidence of illiac crest donor site pain after graft harvest procedures, stimulated introduction of nonautologous interbody fusion materials (15). Some authors have reported better fusion without pain in the graft donor site with bone graft substitutes (16, 17). Donor site pain is quite rare and well tolerated by patients in the results of other studies (18, 19). Pioners of anterior decompression and fusion technique had high rates of pseudoarthrosis and kyphosis in multilevel procedures, what led to the development of an anterior internal fixation device in 1964 (20). From Bohler till now, many different plates divided in three generations, were designed. Unrestrictive backout plates represent the first generation of internal fixation (Fig. 1 upper, lower-left). In second generation, backout of the screws is restricted by locking of screw head

(Fig. 1 lower-center) and plates are designed in two variants: constrained and semiconstrained rotational system. Third generation is dynamic plate, designed as aligment guide that allowes almost 100% of axial graft loading, in order to stimulate natural bone healing (Fig. 1. lower-right). Internal fixation became unavoidable part of every cervical spine fusion, even in one-level decompression (21). The clinition is faced with a burgeoning and bewildering arrey of plate designs, each claiming to secure the best clinical outcome. In view of this uncertainities, it is not surprising that there are substantional variations in the proportion of the patients with cervical spondylotic radiculomyelopathy who are referred for surgery. In addition, appearence of every new and better designed internal fixation system was connected with price increase.

We investigated in a prospective cohort study, firstly, is fusion with 3rd generation dynamic fixation system better than with 1st unrestricted backout plate. Second aim of the study was to answer at the question: is fusion without any augmentation equally effective as with the implants after one level discectomy?

### Patients and Methods

Patients

Beetwen January 2001 and September 2003, 56 patients with spondylogenic radiculopathy and/or myelopathy eligible for the study were referred from the neurosurgical outpatients department to the hospital. During first two years of the study patients were operated  in General Hospital Pula, and during last 9 monthes in Clinical Hospital for Traumatology Zagreb. Their symptoms had not decreased dispite the application of conservative therapy. The indication for surgery treatment

and inclusion criteria were symptoms and signs of compressive radiculopathy or myelopathy. Multilevel patients with cervical kyphosis or negative Ishihara index

(Fig. 2 left) were included in the study. The existence of MRI or CT/myelography confirmed cord and/or nerve root compression was needed for the inclusion in the study (Fig. 2 right). Patients consent to participate in independent clinical and radiographic follow-up was also required. Patients whose primary symptoms were either axial pain and those with a history of previous cervical spine surgery, fracture, tumor, intradural pathology or segmental instability (>3mm) were excluded.

Ethics Committee of the Pula General Hospital approved the clinical trial. Patients were informed about surgical treatement options and offerred nonaugmented fusion after one-level discectomy without need for plating, decompression with fusion augmented with «H» plate as classical surgical technique or augmentation with dynamic internal fixation system that  offers theoretical advantages, but that new internal fixation device is still in clinical research phase. Patients were allowed to choose their type of surgery, and, therefore, allocate them in one of three study groups. According to previous clinical studies results, we planed 23 patients for each augmented group, 10 one-level patients, 8 two-level and 5 multilevel patients (22, 23). Ten one-level patients were planed for non augmented fusion group. Cessation of the study was planed when proposed number of patients in each subgroup will be operated on. Two-year follow-up was planed.

Surgical Treatment

An anterior approach to the cervical spine was performed from the right side. The patients were placed in the supine position. The head was slightly extended and the shoulders were pulled down with the duck tape fixation. Visualization was obtained through a horizontal incision for one and two level decompression and through incision along the medial border of the sternocleidomastoid muscle for multilevel procedure. C-arm was used to confirm the level that will be operated. To obtain sufficient medio-lateral exposure the medial aspects of the longus colli muscles were resected from their attachments to the vertebral body.  After the incision of the anterior longitudinal ligaments, Caspar’s distractor was placed in the vertebrae above and below the segment planed for decompression. Discectomy and/or corpectomy were performed with a high-speed drill. Using an operative microscope, osteophytes and ossification of the posterior longitudinal ligament (OPLL) were removed. Iliac crest autologous bone graft  was inserted under compression. In H-plate group fusion was augmented with first generation Orozso plate (Instrumentarija, Zagreb, Croatia). In dynamic group fusion was augmented with DOC implants (Acromed, Johnson&Johnson, USA). Multilevel decompression was performed with preservation of intermedial vertebra in order to avoid a bridging plate construction. Before wound closure, a lateral X-ray was done to confirm satisfactory graft and implant placement. A cervical orthosis was applied. Paravertebral drain was removed the morning after surgery and the patients were allowed to resume normal activities.

Primary endpoints

Clinical outcomes were assessed using Odom criteria: excellent, good, fair, or poor (24). Patients with excellent outcomes were those in whom the following were demonstrated: a significant reduction and or cessation of pain medication usage, return to full participation in pre-morbid activities, and/ or return to full-time work; additionally significant improvement was demonstrated in subjective pain. Good outcomes had patients with an improvement in subjective pain, an ability to work part time and/ or partially participate in pre-morbid activities, and a diminished requirement for narcotic and/or analgesic medications compared with preoperative dependence. Patients with fair outcomes were those with mild improvements in subjective pain, no change in analgesic/ narcotic use, and only minimal participation in pre-morbid activity and/ or work, while poor outcomes were defined as no reported improvement in pain, no participation in  pre-morbid activities/ work, and increased or same levels of narcotic/ analgesic use.

Neurological outcome was assessed according to difference between preoperative and 2-year follow-up Nurick grade. Nurick grading scale (25) is  based on the degree of difficulty in walking as follows: Grade 0- signs or symptoms of root involvement without evidence of spinal cord disease; Grade 1- signs of spinal cord disease without difficulty in walking; Grade 2- slight difficulty in walking which did not prevent full-time employment; Grade 3- difficulty in walking which prevented full-time employment or the ability to do all housework, but not so severe to require someone help to work; Grade 4- patients able to walk only with someone else’s help or with the aid of a frame; Grade 5- chairbound or bedridden.

Posible improvement in postoperative quality of life was calculated as difference between preoperative and 2-year follow-up patient-based SF-36 grading scele (26-28). Mean results are reported on a transformed scale of 0 to 100, with higher numbers representing better outcomes on 8 Health Scales: Physical Function (PF), Role-Physical (RP), Bodily Pain (BP), General Health (GH), Vitality (V), Social Function (SF), Role-Emotional (RE) and Mental Health (MH).

Secondary endpoints

Two independent researchers evalueted radiographs taken at the end of the surgery, at 6-week and at 2-year  follow-up examination.  Fusion quality was rated according to Tribus grading scale as follows (29): 1- trabeculation and space obliteration (Fig. 3 upper-left), 2 - endplate partially obliterated, 3 - lucent lines < 1mm, 4 - lucent lines > 1mm and  5 - motion on flexion-extension x-ray views.

To determine dynamization of the implants, translation and rotation of the instrumented screws were radiologicaly evaluated. Translation was measured in millimeters as difference of distances between upper and lower screws (Fig. 3 upper-center and right). Rotation of the screws was calculated in grades as the difference between screw-plate angles (Fig. 3 lower-left and center). Placement of the implants was graded on the basis of the following criteria (29): 1, ideal, with screws positioned in the vertebral body and the plate not overlapping an adjacent disc spaces; 2, fair, with the plate overlapping adjacent disc space (Fig. 3 lower-right); and 3, poor, with screws penetrating into the adjacent disc space.

### Masking and follow-up

The patients were included into the study by the first author (MS), according to the inclusion and exclusion criteria and their own consent. Selected patients were referred to the second and third independent investigators (BG and TB), who independently examined patients and checked their questionnaires preoperatively and after 2-year follow-up. In addition, they assesed X-rays according to Tribus criteria. Each patient’s medical records were labeled with patient’s record number and forwarded to the third and fourth independent investigator (MM and BR) for statistical analysis.

Statistical analysis

The following observed parameters were used in the statistical analysis of differences between the groups: clinical outcomes (SF-36 scale, Nurick criteria, and Odom criteria), and radiological outcomes (Translation and rotation of screws, and Tribus grading scale for grading of fusion and placement of implants). For comparisons between groups Student t-test was used.

### Results

From January 3, 2001 to September 22, 2003, 34 male and 22 female patients fullfieled inclusion criteria and were allocated in 3 study groups (Table 1). They underwent anterior cervical decompression and fusion. The mean-age was 52 years (52.6(8.42) for in Dynamic system group and 51 years (51.8(8.06) for “H”plate group. Patients with one-level decompressed from both groups were compared with 10 patients in which non-augmented fusion was performed (six male and 4 female, mean age 50 years (50.2(7.2). Two patients in H-plate group and 1 patient in DOC group were lost for 2-year follow-up examination.

Quality of life according to SF-36 significantly improved following surgery in all studied groups (DOC: preoperatively 52.6%, postoperatively 72.7%, p=0.000001; H-plate: preoperatively 57.2%, postoperatively  74.6%, p=0.000001; NAF: preoperatively 53.5%, postoperatively 75.6%, p=0,000003). There were no significant differences between groups in postoperative total SF-36 values (DOC fixation vs. “H”-plate p=0,408537; “H”-plate vs. NAF p=0,758439; DOC vs. NAF p=0,341247), although in some categories of the test differences were significant (Fig 4).

Clinical outcome according to Odom criteria in all studied patients was graded as excellent or good (Table 2). One patient 7 months following surgery had hardware breakage with translucency greater than 1 mm. CT scan confirmed pseudoarthrosis (Fig. 5.). Following posterior pedicle screw fixation outcome was good.

Patients in all studied groups showed significant neurological improvement. There was a significant improvement in all groups between preoperative and postoperative average Nurick values (Dynamic fixation - “H”-plate p=0.000426; “H”-plate – NAF p=0.000426; Dynamic fixation – NAF p=0.022204). Also, postoperative differences between groups were not significent.

In the DOC group screw rotation was 0° (Table 3). Mean (range) angle of screw rotation in “H”plate group was 7.2° (4.16° to 10.26°). Angles of rotation in one level, two level and multilevel decompression in H-plate fusion subgroups, were 4º, 7º, and 8.9º respectively. Mean (range) translation of the screws in the DOC group was 2.67mm (1.88 to 3.46), while in the “H”plate group translation was no detected.

Fusion grade at 6-week follow-up examination was significantly lower in DOC group (mean(SD Tribus grade= 1.53±0.56), and in Non-augmented fusion group (mean(SD Tribus grade= 1.50±0.51), than in “H”-plate group (mean(SD Tribus grade= 2.13±0.62). One patient in the “H”-plate group had a translucency greater than 1 mm at two-year follow-up examination. Seven patients in the DOC group had heterotopic ossification on the suprajacent segment with ankylosis in 2 patient (Fig. 6. left). In last 10 patients of DOC group internal fixation device was placed in upside-down position to avoid overlapping of adjacent segment with dynamized implants (Fig. 6. center and right). We did not noticed osification of subjacent segment among that 10 patients.

Discussion

Our study showed that there is no difference in clinical outcome between three different typs of fusion following anterior cervical decompression in the tretament of spondylotic radiculomyelopathy. In addition we showed that 1st generation unrestricted backout plates are also dynamic device permiting angular deformation.  Angular dynamization is limited under 10 degrees. Six week follow-up X-rays of the patients with 3rd generation dynamic implants showed lower frequency of visible endplate-bone graft interface. One patient in “H”-plate group underwent posterior transpedicular fixation due to severe neck pain seven months following surgery, with radiological finding of non-union and hardware breakage. Two-year follow-up X-ray of second patient from H plate group showed translucency greater than 1 mm without clinical signs of non-union.

Our study had at least two weaknesses. First, the group of patients included into trial was small, because the study was planed for county hospital where the frequency of surgeries for the treatment of spondylogenic radiculomyelopathies was relatively low.  Second, allocation of the patients was not random but we allowed the patients to chose type of surgery. Randomized Controlled Trials is viewed as the gold standard of clinical research when the goal is to compare the efficacy of various treatment options. We believed that for comparison of different typs of surgeries issues of blinding (for patient, investigators, and treating physicians) and willingness to consent to randomization may limit the scientific validity and practicality of such trials (30) .

All the surgeries were performed by single surgeon what eliminate influence of different surgical techniques. In addition, according to our best knowledge this is the first study that prospectively compared three common anterior cervical fusion techniques. Epstein, Bose, and Steinmetz reported very promising resuts obtained with different typs of dynamic implants in cases series (31-34) Epstein compared fixed with dynamic plate complications in multilevel cervical corpectomy and circumferential fusion technique. Introduction of dynamic plates reduced failure rate and need for secondary posterior fusion from 13% to 3.6%  (35).

Clinical outcome was assessed according surgeon-based outcome scales (Nurick grades and Odom’s criteria) and patient-based outcome scale (SF-36 questionnaire). In the majority of studies, dealing with anterior cervical fusion operative outcome have been evaluated using surgeon-based criteria (36-40). More recently, outcomes have been assesed using patient-based questionnairs, particulary SF-36. Employing the SF-36 to evaluate outcomes of 28 two-level ACDF, Klein at al (41) concluded that the SF-36 revealed significant postoperative improvement on 5 Health Scales: Bodily Pain, Vitality, Physical Function, Role-Physical, and Social Function. Epstein combined surgeon-based measures and SF-36 to evaluate results following single-level ACF procedures performed with fixed and/or dynamic plating system (32, 42, 43). Analysis of three outcome measures in our study, demonstrated that there is no difference between the three studied groups. Huge number of papers about surgical treatment of spondylotic radiculomyelopathy deal with proper selection of implants, in contrary to negligible number of clinical studies about indication for surgery, thoroughness of decompression, or construct design (5, 44-46). Our result suggest that selection of implants is not crucial for clinical outcome.

Wolff’s Law describes bone responds to stress, and suggests that bone heals optimally when exposed to compressive loads. The usefulness of the anterior cervical plate is promotion of fusion by providing stability between the bone graft and donor vertebrae. However, an implant induces reduction of bone healing enhancing loads under plate that can result in non-union. It appears to be an optimal amount of load-sharing between the spinal implant and the bone grafts. Brodke and colleagues showed that in conditions simulating graft subsidence load sharing ratio is more than 4 times better in dynamic  implant group than in plate group (47). Tye and colleagues showed that, in the immediate weeks following instrument-assisted ACF fusion, segment subsides or decreases in the lenght (48).  In the Dynamic group of our study, almost all subsidence occurred in first two days following surgery. Three factors directly affect the incidence and extent of subsidence: 1. the closeness of fit of the bone graft in the vertebral body mortise, 2. the surfface area of contact between the bone graft and vertebral body, and 3. the quality of the contact surfaces. There is a proverbial “race” between the failure of the implant and the acquisition of bony fusion. The capability of an anterior cervical plate to stabilize the spine after three-level corpectomy was significantly reduced with fatique loading (49).  Panjabi et al, (50) showed that there is excessive screw-vertebra motion caused by fatique at the lower end of the three-level corpectomy model. Our results, at six week X rays follow-up  of the patients with 3rd generation dynamic implants, showed lower frequency of visible endplate-bone graft interface at the end of repair stage of bone healing process. These results sugest that normal settling is faster and early bone healing process better with dynamic implants. Unfortunately, we did not planed our study as prospective observational cohort study, and we can not correlate early radiological findings with clinical course.

In our study, patients that needed posterior redo, surgeon-related factors of a poor fit and small bone graft surface area of contact were probably responsible for non-union (Fig 5 right). Rotational dynamization of the “H”-plate was insuficient to allow excessive need for settling caused by poor fit and small surface area of contact. After an anterior cervical plate is applied with the graft under compression, the graft force increases in extension and decreases in flexion, (51) which is opposite to DOC system that offers essentionally no resistance to vertical movement. Resistive strength of the endplate-subhondral bone is estimated to be 200 N. This limits was approached with 5 to 10 degress of extension. The loads required to cause endplate bone failure  approached rapidly within the degrees of motion, occuring in most available cervical orthoses. Application of an anterior cervical plate with suboptimal bone graft creates supraphysiologic loading in extension what is posible explanation of failure in our patient.

One third of the patients with dynamic ossification had suprajacent segment heterotopic ossification which led to ankylosis in two patients. Ankylosis was also recorded in one patient where implant did not overlapp adjacent segment following dynamization

Vertical rods axial telescoping is allowed in upper platform and overlapping of the disc was connected with heterotopic ossification and ankylosis. Delamarter was the single author that reported adjucant level impingment (52). In the last ten patients of the trail group dynamic implant was placed in upside-down position what prevented overlapping of adjacent segment. (Fig. 4 center and right)

Clinical implication of our study is that selection of the internal fixation device must not be main concern of the surgeon in decision making proces. Three patients in NAF group with dislogement of the graft with transient dysphagia in one of them and the two pseudarthrosis in the H plate group, suggest that implant can be recommended in all decompressed patients with selection of dynamic implants for two and more discs decompression. The  reluctance of surgeons to use new design of cervical plate can not be exused with explanation of saving  many for health care delivery system.

Our next step should be study in which possible difference in speed of natural settling and bone healing process will be compared both clinically and radiologically.

Table.1. Demographic, preoperative and follow-up data of patients operateded using instrumented fusion with dynamic fixation (Trial) and fixation with semi constrained cervical plate

| Parameter | Augmented fusion | Non-augmented fusion (graft) |
| --- | --- | --- |
|  | Dynamic | «H»-plate |  |
| Gender (M/F) | 13/10 | 15/8 | 6/4 |
| Age(years) † | 52.6(8.42 | 51.8(8.06 | 50.2(7.2 |
| One-level decompression | 10 | 10 | 10 |
| Two-level decompression | 8 | 8 | 0 |
| Three-level decompression | 5 | 5 | 0 |
| Average Nurick Grades | 0.73(0.70 | 0.67(0.61 | 0.67(0.70 |
| p | 0,784698 vs H-plate | 1,000000 vs NAF | 0,824604 vs Dyn |

† mean ( SD

Table 2. Primary outcome

| Parameter | Augmented fusion | Non-augmented fusion (graft) |
| --- | --- | --- |
|  | Dynamic | «H»-plate |  |
| Average Nurick Grades | 0.13(0.35 (-0.60) | 0.06(0.28 (-0.61) | 0.10(0.32 (-0.57) |
| p | 0,558860 vs H-plate | 0,775019 vs NAF | 0,811457 vs Dynamic |
| p vs preoperative | 0,000426 | 0,000426 | 0,022204 |
| Odom's critreria | Excellent | 13/22 | 14/21 | 7/10 |
|  | Good | 9/22 | 7/21 | 3/10 |
|  | Fair | 0/22 | 0/21 | 0/10 |
|  | Poor | 0/22 | 0/21 | 0/10 |

† mean ( SD

Table 3. Secondary outcome

| Follow-up | Parameter | Augmented fusion | Non-augmented fusion |
| --- | --- | --- | --- |
|  |  | Dynamic | «H»-plate |  |
| 6 weeks | Angle (degree) † | 0 | 7.2±3.04 | - |
|  | Translation (mm) † | 2.67±0.79 | 0 | - |
|  | Implant placement |  |  |  |
|  | Gradus 1 | 15/22 | 21/21 |  |
|  | Gradus 2 | 7/22 | 0/21 |  |
|  | Gradus 3 | 0/22 | 0/21 |  |
|  | Fusion grade † | 1.53±0.56 | 2.13±0.62 | 1.50±0.51 |
|  | p | 0,000028 vs H-plate | 0,000268 vs NAF | 0,861215 vs Dyn |
| 2 years | Fusion grades † | 1.13±0.34 | 1.21±0.52 | 1.1±0.31 |
|  | p | 0,441864 vs H plate | 0,393371 vs NAF | 0,731264 vs Dyn |
|  | Complications | HO N=7 Ankylosis N=2 | 0 | Graft dislodgement N=3 |

† mean ( SD

HO – Heterotopic ossification

Figure legend

Fig. 1 upper: Classification system of anterior cervical plates; lower-left: First generation unrestricted backout plate; lower-center: Second generation restricted backout semiconstrained plate; lower-right: Third generation dynamic plate

Fig. 2 left: Kyphotic cervical spine with negative Ishihara index; right: Spinal cord compression shown by MRI (upper) and CT after myelography (lower)

Fig. 3 upper-left: Trabeculation and space obliteration of upper and lower end-plate                          represent grade 1 fusion according to Tribus classification; upper-center and right: Natural settling under dynamic implants occured in first two postoperative days; lower-left and center: Rotation of 4 degrees was noticed in 6-week follow-up X-ray after two-lewel corporectomy; lower-right: Vertical rods axial telescoping with overlapping of suprajacent segment  induced heterotopic ossification

Fig. 4: Short form 36 showed signifficant improvement in all studied groups, specially in Bodily Pain, Vitality, Physical Function, Role-Physical, and Social Function. There were no differences between 3 studied groups in 2-year follow up results.

Fig. 5 left: CT sagital reconstruction confirmed non-union; right: Poor fit and small bone surface area of contact are surgeon-related factors  responsible for non-union under «H»-plate

Fig. 6 left: Heterotopic ossification with ankylosis of supradjacent segment; center and right: Upside-down placement of dynamic implants in order to prevent  overlapping of adjacent segment following  vertical rods axial telescoping

Acknowledgment.

The Croatian Ministry of Science and Technology (grant No. 0062076 to M. Stančić) financially supported this study. Part of this results will be presented at The Fourth Congress of the Croatian Neurosurgical Society.

###### References

- Young WF. Cervical spondylotic myelopathy: a common cause of spinal cord dysfunction in older persons. Am Fam Physican 2000;62:1064-70

- Pallis C, Jones AM, Spillane JD. Cervical spondylosis: Incidence and implications. Brain 1954,77.274-98.

- Clark E, Robinson PK. Carvical myelopathy: a complication of cervical spondylosis. Brain 1956;79:483-510.

- Fouyas IP, Statham PFX, Sandercock PAG. Cochrane review on the role of surgery in cervical spondylotic radiculomyelopathy. Spine 2002;27:736-47

- Fager CA. Reversal of cervical myelopathy by adequate posterior decompressin. Lahey Clin Found Bull 1969;18:99-108

- Cloward RB, The anterior approach for removal of cervical disks. J Neurosurg 1958;15:602-617

- Smith GW, Robinson RA. The treatment of certain cervical-spine disorders by anterior removal of the intervertebral disc and interbody fusion. J Bone Joint Surg (Am( 1958;40:607-24

- Edwards CC 2nd, Riew KD, Anderson PA. Hilibrand AS, Vaccaro AF. Cervical myelopathy, current diagnostic and treatment strategies. Spine J 2003;3:68-81

- Savolainen S, Rinne J, Hernesniemi J. A prospective randomized study of anterior single-level cervical dusc operations with long-term follow-up: Surgical fusion in unnecessary. Neurosurgery 1998;43:51-5

- Dowd G, Wirth F. Anterior cervical discectomy: Is fusion necessary. J Neurosurg 1999;90(Suppl):8-12

- George B, Gauthier N, Lot G. Multisegmental cervical spondylotic myelopathy and radiculopathy treated by multisegmental oblique corpectomies without fusion. Neurosurgery 1999;44:81-90

- Bertagnoli R, Yue JJ, Pfeiffer F, Fenk-Mayer A, Lawrence JP, Kershaw T, Nanieva R. Early results after ProDisc-C cervical disc replacement. J Neurosurg Spine 2005;2:403-10

- Kaufman HH, Jones E. The principles of bony spinal fusion. Neurosurgery 1989;24.264-9

- Wigfield CC, Nelson RJ. Nonautologous interbody fusion materials in cervical spine surgery: How strong is the evidence to justify their use? Spine 2001;26:687-93

- Heary RF, Schlenk RP, Sachteri TA, Barone D, Brotea C. Persistent iliac crest donor site pain: independent outcome assessment. Neurosurgery 2002;50:510-7

- Samartzis D, Shen FH, Goldberg EJ, An HS. Is autograft the gold standard in achieving radiographic fusion in one-level anterior cervical discectomy and fusion with rigid anterior plate fixation? Spine 2005;30:1756-61

- Thalgott JS, Fritts K, Giuffre JM, Timlin M. Anterior interbody fusion of the cervical spine with coralline hydroxyapatite. Spine 1999;24:1295-9

- Kurz LT, Garfin SR, Booth RE. Harvesting autogenous iliac bone grafts: A review of complications and techniques. Spine 1989;14:1324-31

- Banwart JC, Asher MA, Hassanein RS. Iliac crest bone graft harvest donor site morbidity: A statistic evaluation. Spine 1995;20:1055-60

- Bohler J. (Immediate and early treatment of traumatic paralegias( Z Orthop Ihre Grenzgeb 1967;103:512-29 (German(

- Balabharda RSV, Kim DH, Zhang H-Y. Anterior cervical fusion using dense cancellous allograft and dynamic plates. Neurosurgery 2004;54:1405-12

- Jugovac I, Burgić N, Mićović V, Radolović-Prenc L, Uravić M, Golubović V, Stančić M. Carpal tunnel release by limited palmar incision vs traditional open technique: Randomized controlled trial. Croat Med J 2002;43:33-6

- Ljubičić Bistrović I, Ljubičić Đ, Ekl D, Penezić Lj, Močenić D, Stančić M: Influence of depression on patients satisfaction with outcome of microsurgical “Key-hole” vs classical discectomy: prospective matched cohort study

- Odom GL, Finney W, Woodhall B. Cervical disk lesions. JAMA 1958;166:23-28

- Nurick S. The pathogenesis of the spinal cord disorder associated with cervical spondylosis. Brain 1972;95:87-100

- Jureša V, Ivanković D, Vuletić G, Babić-Banaszak A, Srček I, Mastilica M, Budak A. The Croatian health survey- SF-36: I. General quality of life assessment. Coll Antropol 2000;24:69-78

- Hee HT, Whitecloud TS, Myers L, Gaynor J, Roesch W, Ricciardi JE. SF-36 health status of workers compensation cases with spinal disorders. Spine J 2001;1:176-82

- Grevitt M, Khazim R, Webb J, Mulholland R, Shepperd J. The Short form-36 health survey questionnaire in spine surgery. J Bone Joint Surg (Br( 1997:79B:48-52

- Tribus CB, Corteen DP, Zdeblick TA. the efficiacy of anterior cervical plating in the management of symptomatic pseudoarthrosis of the cervical spine. Spine 1999;24:860-4

- Keller RB, Atlas SJ. Is there a continuing role for prospective observational studies in spine research? Spine 2005;30:847-9

- Epsein NE. Anterior dynamic plates in complex cervical reconstruction surgeries. J Spinal Disord 2002;15:221-8

- Epstein NE. Anterior cervical dynamic ABC plating with single level corpectomy and fusion forty-two patients. Spinal Cord 2003;41:153-8

- Bose B. Anterior cervical arthrodesis using DOC dynamic stabilization implant for improvement in sagittal angulation and controlled settling. J Neurosurg 2003; 98 (1 Suppl):

- Steinmetz MP, Warbel A, Whitfield M, Bingaman W. Preliminary experience with the DOC dynamic cervical implants in the treatment of multipl cervical spondylosis. J Neurosurg Spine 2002;97:330-6

- Epsein NE. Fixed vs dynamic plate complications following multilevel anterior cervical corpectomy and fusin with posterior stabilization. Spinal Cord 2003;41:379-84

- Vaccaro AR, Falatyn SP, Scuderi GJ, Eismont FJ, McGuire RA, Singh K, Garfin SR. Early failure of long segment anterior cervical plate fixation. J Spinal Disord 1998;11:410-5

- Saunders RL, Pikus HJ, Ball P. Four-level cervical corpectomy. Spine 1998;23:2455-61

- Fessler RG, Steck JC, Giovanini MA. Anterior cervical corpectomy for cervical spondylotic myelopathy. Neurosurgery 1998;43:257-65

- Eleraky MA, Llanos C, Sonntag VK. Cervical corpectomy: report of 185 cases and review of the literature. J Neurosurg 1999;90(1 Suppl):35-41

- Macdonald RL, Fehling MG, Tator CH, Lozano A, Fleming JR, Gentili F, Bernstein M, Wallace MC, Tasker RR. Multilevel anterior cervical corpectomy and fibular allograft fusion for cervical myelopathy. J Neurosurg 1997;86:990-7

- Klein GR, Vaccaro AR, Todd JR. Health outcome assessment before and after anterior cervical discectomy and fusion for radiculopathy: A prospective analysis. Spine 2000;25:801-3

- Epsein NE. The management of 1 level anterior cervical corpectomy with fusion employing Atlantis hybrid plates: preliminary experience. J Spinal Disord 2000;13:324-8

- Epsein NE. The efficacy of anterior dynamic plates in complex cervical surgery. J Spinal Disord Tech 2002;15:221-7

- Teresi LM, Lufkin RB, Reicher MA, Foffit BJ, Vinuela FV, Wilson GM, Bentson JR, Hanafee WN. Asymtomatic degenerative disk disease and spondylosis of the cervical spine: MRI imaging. Radiology 1987;164:83-8

- Riew KD, McCulloch JA, Delamarter RB, An HS, Ahn NU: Microsurgery for degenerative conditions of the cervical spine. Instr Course Lect 2003;52:497-508

- Singh K, Vaccaro AR, Kim J, Lorenz EP, Lim T-H, An HS. Enhancement of stability following anterior cervical corpectomy: A biomechanical study. Spine 2004;29:845-9

- Brodke DS, Gollogy S, Mohr A, Nguyen B-K, Dailey AT, Bachus KN. Dynamic cervical plates: Biomechanical evaluation of load sharing and stiffness. Spine 2001;26:1324-9

- Tye GW, Graham RS, Broaddus WC, Young HF. Graft subsidence after instrument-assisted anterior cervical fusion. J Neurosurg 2002; 97(2 Suppl):186-92

- Isomi T, Panjabi MM, Wang J-L, Vaccaro AR, Garfin SR, Patel T. Stabilizing Potential of anterior cervical plates in multilevel corpectomies. Spine 1999;24:2219-23

- Panjabi MM, Isomi T, Wang J-L. Loosening at the screw-vertebra junction in multilevel anterior cervical plate constructs. Spine 1999;24:2283-8

- DiAngelo DJ, Foley KT, Vossel KA, Rampersaund YR, Jansen TH. Anterior cervical plating reverses load transfer through multilevel strut-grafts. Spine 2000;25:783-95

- Delamarter R, Bae H. anterior dynamic plating for cervical fusions analysis of clinical failures. Eurospine 2004, Porto, Portogalo: Poster #20