THERMAL DEGRADATION BEHAVIOUR OF POLY(3-HYDROXYBUTYRATE)/CLOISITE 30B NANOCOMPOSITES

M. Erceg, T. Kovačić, I. Klarić

Department of Organic Technology, Faculty of Chemistry and Technology, Teslina 10/V, 21 000 Split, Croatia (merceg@ktf-split.hr)

Poly(3-hydroxybutyrate) (PHB) is a fully biodegradable thermoplastic which has recently drawn much attention as an environmentally harmless alternative to petrochemical derived plastics. However, there is no large commercial production of PHB products because of its very low thermal stability at processing temperatures, pronounced brittleness and high cost. Recently developed nanocomposites consisting of a polymer and only a few percent of layered silicates as environmentally friendly nanofillers, often exhibit improved thermal, mechanical and other properties when compared to pure polymers and conventional composites.

This investigation is focused on the preparation of polymer nanocomposites of PHB with organically modified montmorillonite Cloisite 30B (30B), the effects of Cloisite 30B loading on the thermal stability of PHB and the determination of kinetic parameters and mechanism of their non-isothermal degradation.

PHB/30B nanocomposites with compositions 100/0, 100/1, 100/3, 100/5, 100/7 and 100/10 by weight were prepared by solution intercalation method.

The non-isothermal thermogravimetric analysis of PHB/30B nanocomposites was carried out over the temperature range 50-500°C at four heating rates (2,5; 5; 10 and 20°Cmin-1) in the nitrogen atmosphere.

The onset decomposition temperatures (T°) and the temperatures at the maximal degradation rate (Tmax) of PHB/30B 100/1, 100/3 and 100/5 are higher compared to pure PHB and therefore their thermal stability is improved. Sample PHB/30B 100/7 shows similar and sample PHB/30B 100/10 lower values of T° and Tmax compared to pure PHB.

The invariant kinetic parameters method1 (IKP) was used in combination with isoconversional methods (Flynn-Wall-Ozawa2 and Kissinger-Akahira-Sunose3) to determine the kinetic triplet for the PHB/30B non-isothermal degradation, i.e. the activation energy (E), the pre-exponential factor (A) and the conversion function f(a). By means of isoconversional methods, E and its dependence on conversion (a) are obtained. The values of Einv and Ainv obtained by IKP method were used for numeric evaluation of f(a). The dependence of f(a) vs. a can not be fitted precisely by any ideal kinetic model but its shape suggests the true f(a) characteristic. Finally, the true kinetic triplets for the non-isothermal degradation of each PHB/30B nanocomposite were obtained.

References

1) A.I. Lesnikovich, S.V. Levchik J Therm Anal, 1983, 27, 89.

2) T. Ozawa, Thermochim. Acta, 1992, 203, 159.

3) T. Akahira, T. Sunose Res Report Chiba Inst Technol., 1971, 16, 22.