KINETIC ANALYSIS OF THE ISOTHERMAL DEGRADATION OF PHB/OMMT NANOCOMPOSITES

Matko Erceg*, Tonka Kovačić, Ivka Klarić

Faculty of Chemistry and Technology, Department of Organic Technology,

Teslina 10/V, 21 000 Split, Croatia

* E-mail: merceg@ktf-split.hr; tel: ++ 385 21 329 459; fax: ++385 21 329 461

Polymer nanocomposites consisted of biodegradable poly(3-hydroxybutyrate) (PHB) and organically modified montmorillonite Cloisite25A (OMMT) as nanofiller with compositions PHB/OMMT 100/0, 100/1, 100/3, 100/5, 100/7 and 100/10 by weight were prepared by solution intercalation method [1]. These samples were degraded isothermally for 120 min at 230, 235, 240 and 245ºC in the nitrogen atmosphere. The addition of OMMT increases the thermal stability of PHB. The most pronounced effect has the addition of 7 wt. % of OMMT where the occurrence of the constant mass plateau is shifted for 30 min to longer degradation times compared to pure PHB.

The kinetic triplets (activation energy, E; pre-exponential factor, A; kinetic model g()) of the isothermal thermogravimetric (TG) degradation of pure PHB and PHB/OMMT nanocomposites are obtained without making any assumption about g(). For the determination of kinetic triplets the so called reduced time plots (RTP) method is used. This method is broadly used in solid state kinetics [2]. Each theoretical g() [3] has unique RTP plot and the true g() of the investigated process can be obtained by comparison of the experimental RTP curves with the theoretical ones. Isothermal degradation of PHB/OMMT nanocomposites occurs through mechanism described with Avrami-Erofeev kinetic model g()=[-ln(1-)]1/n. To calculate the values of parameter n, i.e. empirical kinetic models, this expression is introduced into logarithmic form of general kinetic equation, lnt = ln[g()] -lnk. From the slope and intercept of the plots lnt vs. ln[-ln(1-)] parameter n and reaction rate constants, lnk for each degradation temperature are obtained, respectively. By plotting -lnk vs. 1/T, a straight line is obtained and from its slope and intercept E and lnA are calculated, respectively. The values of kinetic triplets (E, lnA, g()) obtained by RTP method are shown in Table 1. Eiso values are obtained by model-free integral isoconversional method, i.e. without assumption of g(). The results in Table 1 show that E values obtained by RTP method are almost identical to Eiso values, what proofs the correctness of kinetic analysis.

Table 1. Values of kinetic parameters obtained by RTP and integral isoconversional methods

| PHB/25A | Conversion,  | g() | E / kJmol-1 | lnA / min-1 | r2 | Eiso / kJmol-1 |
| --- | --- | --- | --- | --- | --- | --- |
| 100/0 | 10-90 | [-ln(1-)]1/3,33 | 111,1 | 23,0961 | 0,99482 | 107,9 |
| 100/1 | 10-90 | [-ln(1-)]1/3,54 | 136,9 | 29,0116 | 0,99581 | 136,3 |
| 100/3 | 30-90 | [-ln(1-)]1/4,28 | 123,7 | 25,8440 | 0,99818 | 123,4 |
| 100/5 | 30-90 | [-ln(1-)]1/3,98 | 118,8 | 24,5619 | 0,99669 | 118,8 |
| 100/7 | 30-90 | [-ln(1-)]1/3,15 | 101,5 | 20,2266 | 0,99769 | 101,9 |
| 100/10 | 40-90 | [-ln(1-)]1/1,99 | 96,7 | 19,6063 | 0,99429 | 97,5 |

[1] M. Erceg, T. Kovačić, I. Klarić, J. Appl. Poly, Sci. (in press)

[2] S. Vyazovkin, C. A. Wight, Thermochim. Acta 340-341 (1999) 53-68.

[3] K. Pielichowski, J. Njuguna, Thermal Degradation of Polymeric Materials, Rapra

Technology, Shawbury, 2005, pg. 40.