<one empty line>

π-Interactions of quinoid rings in the solid state

<one empty line>

Krešimir Molčanov, Biserka Kojić-Prodić

<one empty line>

π-Interactions of aromatic molecules are well-known and were extensively studied [1,2]. The aromatic rings stack either as parallel and offset (Fig. 1a) or T-shaped (Fig. 1c); in such arrangements σ-π attractions outperform π-π repulsions. However, parallel, face-to-face arrangement (Fig. 1b) is energetically unfavourable due to strong repulsion of π electrons.

Figure 1 Possible arrangements of planar rings: a) parallel, offset and b) T-shaped are energetically favourable for aromatic molecules; c) parallel, face-to-face is unfavourable. d) An experimentally observed stack of hydrogen chloranilate anions in the crystal structure of potassium hydrogen chloranilate dihydrate [3]. Green arrows indicate σ-π attraction, while red arrows indicate π-π repulsion.

π-Interactions of quinoid molecules were little studied. Recently, we discovered that some substituted 2,5-dihydroxyquinones stack face-to-face in crystals [3-5]; distances between centroids of contiguous rings are 3.2 - 3.4 Å, which is significantly shorter than the sum of van der Waals radii (for carbon it is 3.5 Å), and also much shorter than distances in aromatic stacks (typically 3.65 - 4.3 Å). Quantum-chemical calculations indicate unusually strong dispersion interactions with energies of about 20 kcal mol-1 being comparable to strong hydrogen bonds. The electronic structure of quinoid rings is in favour of face-to-face stacking; π electrons are not delocalised (as in aromatics), but distinguishable single and double bonds exist. Therefore, π-π repulsion is minimised and σ-π attraction maximised in parallel, face-to-face arrangement. Such interactions have a great potential in crystal engineering and design of functional materials.

[1] C. A. Hunter, K. R. Lawson, J. Perkins, C. J. Urch, J. Chem. Soc., Perkin Trans., 2001, 2, 651.

[2] L. M. Salonen, M. Ellermann, F. Diedrich, Angew. Chem., Int. Ed., 2011, 50 , 4808.

[3] K. Molčanov, B. Kojić-Prodić, A. Meden, CrystEngComm, 2009, 11, 1407.

[4] K. Molčanov, B. Kojić-Prodić, CrystEngComm, 2010, 12, 925.

[5] K. Molčanov, I. Sabljić, B. Kojić-Prodić, CrystEngComm, 2011, 13, 4211.