# MICROSTRUCTURAL CHARACTERIZATION OF Ti-BASED ALLOYS

# MIKROSTRUKTURNA KARAKTERIZACIJA LEGURA NA BAZI TITANA

# Ljerka Slokar*, Tanja Matković, Prosper Matković

University of Zagreb Faculty of Metallurgy, Department for Physical Metallurgy

Aleja narodnih heroja 3, 44103 Sisak, Croatia

*e-mail: slokar@simet.hr

Abstract:

In a few last decades development of biomedical titanium alloys without undesirable elements, aluminium and vanadium, has continued to increase. This paper shows microstructural characterization of two groups of titanium-based alloys. First, titanium was alloyed with chromium and molybdenum. In second type, niobium and zirconium were added to titanium. Purpose of this investigation was to examine the microstructure and hardness of Ti-Cr-Mo and Ti-Nb-Zr alloys with potential for biomedical use. Chemical compositions of investigated alloys were selected fro, the same corner of ternary titanium rich diagram and according to the similar biomedical Ti-based alloys. Three samples with different composition of each alloy type were laboratory prepared by an arc melting method. Their microstructure was examined by scanning electron microscope with energy-dispersive spectrometer (EDS) by point and line analysis. Hardness was determined by Vickers method. Results show that Ti-Cr-Mo alloys have two-phases microstructure containing β and ( or (” phase, while Ti-Nb-Zr alloys were nearly β single-phase with traces of (-phase. EDS analysis indicates that ( and β have similar chemical composition which is in a good agreement to alloy composition. Vickers hardness of Ti-Cr-Mo alloys increases with molybdenum content, while those for Ti-Nb-Zr alloys increases with niobium content. According to the closely single-phase microstructure and lower hardness, Ti-Nb-Zr alloys have adventage as potential biomedical materials.

Key words: Ti-based alloys, biomedical material, microstructure, Vickers hardness

Sažetak:

U zadnje vrijeme sve se više razvijaju legure titana za biomedicinsku primjenu koje ne sadrže nepoželjne elemente, aluminij i vanadij. Ovaj rad prikazuje mikrostrukturnu karakterizaciju dvije skupine legura na bazi titana. U prvoj je titan legiran s kromom i molibdenom, a u drugoj su titanu dodani niobij i cirkonij. Svrha ovog rada je ispitati mikrostrukturu i tvrdoću Ti-Cr-Mo i Ti-Nb-Zr legura za potencijalnu primjenu u biomedicini. Kemijski sastavi istraživanih legura odabrani su iz istog dijela ternarnog faznog dijagrama bogatog titanom, te prema sličnim biomedicinskim legurama na bazi titana. Po tri uzorka različitog sastava od svake skupine legura laboratorijski su pripremljeni u lučnoj peći. Njihova mikrostruktura je ispitana skenirajućim elektronskim mikroskopom s energijsko-disperzivnim spektrometrom. Analiza sastava provedena je analizom u točki i linijskom analizom. Tvrdoća je određena Vickersovom metodom. Rezultati pokazuju da su Ti-Cr-Mo legure dvofazne, odnosno da sadrže β i ( ili (“ fazu, dok su Ti-Nb-Zr legure uglavnom β-jednofazne s (-fazom u tragovima. EDS analiza je pokazala da ( ((“) i β faze imaju vrlo sličan kemijski sastav, koji odgovara sastavu legure. Tvrdoća prema Vickersu Ti-Cr-Mo legura povećava se s udjelom molibdena u leguri, dok se ona za Ti-Nb-Zr legure povećava s udjelom niobija. Zbog skoro β-jednofazne mikrostrukture i niže tvrdoće u odnosu na Ti-Cr-Mo legure, Ti-Nb-Zr legure imaju veći potencijal za primjenu kao biomedicinski materijali.

Ključne riječi: legure na bazi titana, biomedicinski materijali, mikrostruktura, tvrdoća prema

Vickersu

- INTRODUCTION

Due to their light weight, excellent mechanical properties and corrosion resistance, titanium alloys are popularly used today in many medical applications. The most widely used titanium biomedical alloy is Ti-6Al-4V. But, since aluminium and vanadium are known to might cause some long-term health problems, alternative Ti-based alloys without toxic elements have been developed [1-3].

The goal of this study was to prepare a new titanium-based alloys with potential for biomedical use. Chromium is a β-eutectoid element, which stabilizes β-phase of titanium. Besides, it is cheap and decreases Young's modulus in a manner similar to niobium as β-isomorphous element in a Ti-Nb alloys. Zirconium suppress the athermal ω-phase produced during quenching and as a result decreases Young's modulus to be similar to the cortical bone (4-30 GPa) [4,5].

- MATERIALS AND METHODS

In this paper two types of titanium alloys were prepared with purpose to examine and compare their microstructure and hardness which would satisfy conditions for biomedical applications.

First, titanium was alloyed with chromium and molybdenum. In second type, niobium and zirconium were added to titanium. Cr and Mo were chosen as a β-stabilizers as well as zirconium and niobium, which are not toxic and do not cause allergic reactions in body tissue [6-8]. Chemical compositions of experimental alloys were selected according to the similar biomedical Ti-based alloys [4,10,11]. Their positions in the portion of isothermal sections of ternary diagrams at the room temperature are presented in Figure 1.

(a) Ti-Cr-Mo alloys			                 (b) Ti-Nb-Zr alloys

Figure 1. Chemical compositions of investigated alloys

Alloys were prepared by melting a pure elements (with purity better than 99.9%) in vacuum arc-furnace under argon atmosphere (Fig.2.). Because of large difference in melting temperature of elements in Ti-Cr-Mo system, first chromium and molbdenum were melted into a „button-shape“ (Fig.2.). These buttons were remelted for a three times, and then titanium was added. Such samples were remelted for another four times to ensure their homogeneity. In the similar way Ti-Nb-Zr alloys were prepared. Namely, niobium and zirconium were remelted for three times, and then titanium was added.

Figure 2. Laboratory arc-furnace and „button-shaped“ alloys in copper mould

Alloys in forms of buttons of approximately 7g were casted in the same equipment by means of specially constructed water-cooled copper anode, which served as a casting mould. In this way, as-cast cylindrical specimens with dimensions 8 mm x 25 mm were produced and they were sectioned using a Buehler Isomet low-speed diamond saw. After embedding in conductive resin Conductomet, specimens were metallographically prepared by grinding and polishing. The microstructure of two Ti-Cr-Mo alloys (No. 2 and 3) was remarked easily, but there was a need for etching another samples. Microstructural analysis was performed using a scanning electron microscope (SEM) Tescan Vega TS 5136 MM with Bruker energy-dispersive spectrometer (EDS) by point and line analysis. Hardness of as-cast experimental alloys were determined by Vickers method with load 19.60N for 10 s.

- RESULTS AND DISCUSSION

Microstructure and hardness of Ti80Cr10Mo10, Ti70Cr20Mo10, Ti70Cr10Mo20 and Ti80Nb10Zr10,  Ti70Nb20Zr10, Ti70Nb10Zr20 respectively, were examined. SEM analysis of three Ti-Cr-Mo as-cast alloys showed that all of them have two-phases microstructure (Fig.3). Alloy Ti80Cr10Mo10 with highest titanium content after etching revealed a white needles of (''-phase in a matrix of β-phase. Other two non-etched alloys showed a dark dendrites of (-phase in a matrix of β-phase.

(a) Ti80Cr10Mo10               		            	(b) Ti70Cr20Mo10

(c) Ti70Cr10Mo20

Figure 3. SEM micrographs of investigated Ti-Cr-Mo alloys

with EDS spectrum of phases

SEM micrographs of Ti-Nb-Zr alloys (Fig.4) show β-matrix and probably the presence of (-phase according to the reference [1].

(a) Ti80Nb10Zr10                                                       (b) Ti70Nb20Zr10

(c) Ti70Nb10Zr20

Figure 4. SEM micrographs of investigated Ti-Nb-Zr alloys

with EDS spectrum of phases

Chemical compositions of all phases were determined by EDS point analysis (Table 1).

# Table 1. EDS results obtained by point analysis

| No. | Alloy composition, at.% | Element | Elements content in |
| --- | --- | --- | --- |
|  |  |  | β-phase, at.% | (-phase, at.% |
| 1. | Ti80Cr10Mo10 | Ti | 80 | 80 (α'') |
|  |  | Cr | 9 | 9 (α'') |
|  |  | Mo | 11 | 11 (α'') |
| 2. | Ti70Cr20Mo10 | Ti | 72 | 89 |
|  |  | Cr | 16 | 7 |
|  |  | Mo | 12 | 4 |
| 3. | Ti70Cr10Mo20 | Ti | 70 | 92 |
|  |  | Cr | 10 | 3 |
|  |  | Mo | 20 | 5 |
| 1. | Ti80Nb10Zr10 | Ti | 81 | - |
|  |  | Nb | 9 | - |
|  |  | Zr | 10 | - |
| 2. | Ti70Nb20Zr10 | Ti | 72 | - |
|  |  | Nb | 19 | - |
|  |  | Zr | 9 | - |
| 3. | Ti70Nb10Zr20 | Ti | 70 | - |
|  |  | Nb | 7 | - |
|  |  | Zr | 23 | - |

These results revealed very similar data for composition of β-phase which mainly corresponds to the alloy composition. The composition of β and (’’-phases are equal for Ti80Cr10Mo10 alloy. This suggests that during an alloys casting with the fast cooling rate the phase transformation occurred, without change in composition (Fig.5a), as the evidence of martensitic transformation β((’’.

(a) Ti80Cr10Mo10                         (b) Ti70Cr20Mo10                        (c) Ti70Cr10Mo20

Figure 5. Elements line distribution in Ti-Cr-Mo alloys

In Ti70Cr20Mo10 and Ti70Cr10Mo20 alloys (-phase contains  much higher titanium ratio which can be clearly seen in Figs.5b and 5c obtained by line analysis.

SEM and EDS analysis of Ti-Nb-Zr alloys showed that all of them have homogenous structure of β-phase (Fig.4). Chemical composition determined in all points revealed the same data, which corresponds to alloy compostion (Table 1). Also, line analysis (Fig.6) showed uniformly line distribution of elements.

(a) Ti80Nb10Zr10                          (b) Ti70Nb20Zr10                        (c) Ti70Nb10Zr20

Figure 6. Elements line distribution in Ti-Nb-Zr alloys

The Vickers hardness measurements (Table 2) show the strong effect of chemical composition and microstructure on hardness values. Obtained data for Ti-Cr-Mo alloys were in the range of 449 to 555 HV2 and they were increased with increasing molybdenum content. So, the highest value of 555 HV2 has alloy Ti70Cr10Mo20.

# Table 2. Vickers hardness of experimental alloys

| No. | Alloy composition, at.% | HV2 |
| --- | --- | --- |
| 1. | Ti80Cr10Mo10 | 449 |
| 2. | Ti70Cr20Mo10 | 542 |
| 3. | Ti70Cr10Mo20 | 555 |
| 1. | Ti80Nb10Zr10 | 379 |
| 2. | Ti70Nb20Zr10 | 474 |
| 3. | Ti70Nb10Zr20 | 411 |

Hardness of Ti-Nb-Zr alloys has lower values (379 – 474 HV2) when compared with Ti-Cr-Mo alloys. This could be explained by fact that β-phase has lower hardness than (-phase [12]. Measured values are similar to that of other titanium β-type biomedical alloys [11,13,14].

- CONCLUSIONS

In this paper two types of titanium-based alloys for biomedical application were studied. From the obtained results it can be concluded as follows:

- SEM analysis shows two-phases microstructure of Ti80Cr10Mo10, Ti70Cr20Mo10 and Ti70Cr10Mo20 alloys, which consists of β and ( or (’’ phases.

- As-cast alloys Ti80Nb10Zr10, Ti70Nb20Zr10 and Ti70Nb10Zr20 were single β-phases.

- EDS indicated that chemical composition of β and (’’ phases are equal for Ti80Cr10Mo10 alloy. This is the evidence that martensitic transformation β(('' takes place.

- Vickers hardness of Ti-Cr-Mo alloys depends on molybdenum content, and that of Ti-Nb-Zr alloys depends on niobium content.

- Hardness of Ti-Nb-Zr alloys are lower than that for Ti-Cr-Mo alloys because the β-alloys has lower hardness than β/( alloys.

According to the results showing single-phase microstructure and lower hardness, Ti-Nb-Zr alloys have advantage in front of Ti-Cr-Mo alloys as potential biomedical materials.

- REFERENCES

- D.J. Lin, J.H. Chern Lin, C.P. Ju, Effect of chromium content on structure and mechanical properties of Ti-7.5Mo-xCr alloys, Journal of Materials Science: Materials in Medicine 14 (2003) 1-7

- E. Eisenbarth, D. Velten, M. Müller, R.Thull, J. Breme, Biocompatibility of β-stabilizing elements of titanium alloys, Biomaterials 25 (2004) 5705-5713

- W-F. Ho, C-H. Pan, S-C. Wu, H-C. Hsu, Mechanical properties and deformation behavior of cast binary Ti-5Cr-xFe alloys, Journal of Alloys and Compounds 472 (2009) 546-550

- M. Geetha, A.K. Singh, R. Asokamani, A.K. Gogia, Ti based biomaterials, the ultimate choice for orthopaedic implants – A review, Progress in Materials Science 54 (2009) 397-425

- Y. Murayama, S. Sasaki, H. Kimura, A. Chiba, Phase stability and mechanical properties of Ti-Cr based alloys with low Young's modulus, Materials Science Forum 654-656 (2010) 2114-2117

- I. J. Polmear, Light Alloys, Metallurgy of the light metals, Third Edition, Arnold, London, 1995.

- L. J. Xu, Y. Y. Chen, Zh. G. Liu, F. T. Kong, The microstructure and properties of Ti-Mo-Nb alloys for biomedical application, Journal of Alloys and Compounds 453 (2008) 320-324

- M. Lamirand, J-L. Bonnentien, G. Ferrière, S. Guérin, J-P. Chavalier, Relative effects of chromium and niobium on microstructure and mechanical properties as a function of oxygen content in TiAl alloys, Scripta Materialia 56 (2007) 325-328

- M. Niinomi, T. Akahori, T. Takeuchi, Sh. Katsura, H. Fukui, H. Toda, Mechanical properties and cyto-toxicity of new beta type titanim alloy with low melting points for dental applications, Materials Science and Engineering C, 25 (2005) 417-425

- W-F. Ho, S-C. Wu, H-H. Chang, H-C. Hsu, Structure and mechanical properties of Ti-5Cr based alloy with Mo addition, Materials Science and Engineering C 30 (2010) 904-909

- Lj. Slokar, T. Matković, P. Matković, Alloying and heat treatment effects on the microstructure and hardness of biomedical titanium alloys, International Conference Proceedings of MATRIB2011, Vela Luka, Croatia, 2011, 450-456

- I. Weiss, S.L. Semiatin, Thermomechanical processing of beta titanium, Materials Science and Engineering A, 243 (1998) 46-65

- M. Koike, M. Itoh, O. Okuno, K. Kimura, O. Takeda, T.H. Okabe, T. Okabe, Evaluation of Ti-Cr-Cu alloys for dental applications, Journal of Materials Engineering and Perfomance 14 (2005) 778-783

- H-C. Hsu, S-C Wu, T-Y. Chiang, W-F. Ho, Structure and grindability of dental Ti-Cr alloys, Journal of Alloys and Compounds 476 (2009) 817-825