Photovoltaic Technical Conference - Thin Film & Advanced Silicon Solutions 2012 -

Amorphous-nanocrystalline silicon thin films for single and tandem solar cells

# D.Gracin1, K.Juraić1, I.Djerdj1, A.Gajović1, S.Bernstorff2, V. Tudić3 and M.Čeh,4

1Rudjer Boškovic Institute, Bijenička 54, 10000 Zagreb, Croatia

2Sincrotrone Trieste, SS 14, km 163.5, 34012 Trieste, Italy

# 3University of Applied Science, Trg J.J. Strossmayera 9, Karlovac, Croatia

4Jožef Stefan Institute, Jamova 39, 1000 Ljubljana, Slovenia

1) Context / Study motivation

The optical properties of amorphous-nano-crystalline thin films deposited by Plasma Enhanced Chemical Vapor Deposition (PECVD) were studied in correlation with the size distribution of individual crystal sizes and the crystalline to amorphous fraction. A possible application as active part in solar cells was tested by integrating the actual Si layers in a typical p-i-n solar cell structure and by computer modeling.

2) Description of approach and techniques

The nano-structural properties were examined by Grazing Incidence Small-Angle X-ray Scattering (GISAXS), Grazing Incidence Wide Angle X-ray scattering (GIWAXS) and High-Resolution Electron Microscopy (HRTEM). X-ray scattering measurements were done at the Austrian SAXS beam-line [1] (Synchrotron Elettra, Trieste). The in-depth size distribution of the nano-crystals was found either uniform across the sample, or the crystals were slightly larger when located closer to the surface [2]. Typical sizes were between 3 and 10 nm while the crystal fraction varied from 15 to 40 vol. %. The crystals remain as individual in amorphous matrix (Fig.1) enabling quantum size effects related to small dimensions of crystals. However, the distribution of crystals sizes was broad and log-normal type (Fig.2) assuming random growth and crystallization [3]. Measurements of the optical properties showed that the spectral distribution of the absorption coefficient in a whole range of crystal to amorphous fractions remained close to pure amorphous silicon in the visible part of the spectrum and showed square dependence on the photon energy (Tauc gap) [4] . The average optical gap was larger for smaller nano-crystals and a higher crystal fraction just confirming the quantum size effects that correspond to quantum dots.

3) Results / Conclusions / Perspectives

The spectral response of solar cells with the examined thin films as active elements showed a narrower spectral distribution and a blue shift comparing to pure amorphous solar cells and micro-crystalline as well (Fig.4). The effect was larger for samples with a higher nano-crystal fraction and smaller crystals suggesting a possible application in multi-layer solar cells. This possibility was tested by computer simulation using AMPS program. The results were higher efficiency than amorphous-microcrystalline tandem cells due to higher optical gap (higher output voltage) and better fill factor (higher mobility).

Figure 1: Typical HRTEM micrograph of a-nC-Si

Figure 2. Characteristic size distribution of nano-crystals

Figure 3.Distribution of absorption coefficient of a-nC-Si (red dots and line), amorphous Si (blue line) and monocrystal Si (black line)

Figure 4.  Quantum efficiency of nC-Si (red line), amorphous Si (black line) and micro crystalline Si (magenta line)

REFERENCES:

[1]	H.Amenitsch, S. Bernstorff, and P. Laggner, High-flux beamline for small-angle x-ray scattering at ELETTRA. Review of Scientific Instruments, vol. 66(2), pp. 1624-1626, 1995.

[2]	D.Gracin, S. Bernstorff, P. Dubček, A. Gajović, K. Juraić,  Study of amorphous nanocrystalline thin silicon films by grazing-incidence small-angle X-ray scattering. Journal of Applied Crystallography,vol. 40, pp. S373-S376, 2007.

[3]	Espiau de Lamaëstre, R. and H. Bernas, Significance of lognormal nanocrystal size distributions. Physical Review B,.vol. 73(12): pp. 125317-125326, 2006.

[4]	D.Gracin, A.Gajović, K.Juraić, M.Čeh, Z.Remeš, A.Poruba, M.Vanecek, Spectral response of amorphous-nanocrystalline silicon thin films, Journal of Non-Cryst. Solids, vol 354 (19-25). pp. 2286-2290, 2008.