## Slide 1: Stacking of planar conjugated rings – beyond aromatics
Krešimir Molčanov
Rudjer Bošković Institute
Zagreb, Croatia

## Slide 2
13th Slo-Cro Crystallographic Meeting, Bovec, 2004.

## Slide 3
15th Slo-Cro Crystallographic Meeting, Jezersko, 2006.

## Slide 4: Potassium hydrogen chloranilate dihydrate
space group
P 21/c
17th Slo-Cro Crystallographic Meeting, Ptuj, 2008.

## Slide 5: KHCA∙2H2O
P 21/c
0
b
a
Molčanov, Kojić-Prodić, Meden, CrystEngComm, 2009, 11, 1407.

## Slide 6: KHCA∙2H2O
Centroid distance:
3.229(2) Å
Offset ≈ 0.2 Å
P 21/c
Molčanov, Kojić-Prodić, Meden, CrystEngComm, 2009, 11, 1407.
c

## Slide 7: Is it because of stacking?
c
Molčanov, Jelsch et al., CrystEngComm, 2015, 17, 8645.

## Slide 8: (Pre)history
Landauer & McConnel, J. Am. Chem. Soc., 1952, 74, 1221.
In 1930’s: porphyrines forming layers; charge transfer
J. Chem. Soc., 1937

## Slide 9: What is it?
In chemistry, pi stacking (also called π–π stacking) refers to attractive,
noncovalent interactions between aromatic rings, since they contain
pi bonds.
Is it dispersion?
It is interaction of quadrupolar moments?
Is it charge transfer?
Is it overlap of π-orbitals?
Is it magnetic interaction due to ‘ring currents’?
How to name it? π∙∙∙π interaction, π-interaction,
aromatic interaction, π-stacking, σ-π stacking…
From Wikipedia:

## Slide 10: Common misconceptions
It occurs only between aromatic rings
It is a weak interaction (E < 1 kcal mol-1)
In crystal packing it plays a ‘second fiddle’ to stronger interactions such as hydrogen bonding
It can’t be used in crystal engineering

## Slide 11
Look, these coins stack!
That means gold is aromatic!
An amazing discovery,
your majesty! It could
win us an IgNobel prize!

## Slide 12: Temple of Hera, Selinunte, Sicily built ca. 460 B.C.
1,2 x 1011 Å

## Slide 13: Temple of Hera, Selinunte, Sicily built ca. 460 B.C.

## Slide 14
Typical centroid
distance:
> 3,8 Å
Offset typically
1,7 – 1,8 Å
Hunter & Sanders, JACS, 1990, 112, 5525.
Hunter, Singh, Thornton, J. Mol. Biol, 1991, 208, 837.
Stacking of aromatic rings
Attraction
Repulsion
offset
α

## Slide 15: A simple explanation: quadrupolar moments
C. Janiak, J. Chem. Soc., Dalton Trans., 2000, 3885-3896.

## Slide 16
δ+
δ+
δ-
δ-
σ∙∙∙π attraction
π∙∙∙π repulsion
σ∙∙∙π attraction
Aromatic π-interactions:
quadrupolar moments

## Slide 17: Rethinking the term „pi-stacking”
Martinez & Iverson, Chem. Sci., 2012, 3, 2191.

## Slide 18
Geometric parameters for description of stacking
α
Cg∙∙∙Cg
∙
β
CgI_perp
offset
Offset = Cg∙∙∙Cg∙sin(β)
Calculated by PLATON:

## Slide 19
Aromatic rings:
tetrachlorohydroquinone
ρmax = 0.034 e Å-1
3.50 Å
3.55 Å
Cg…Cg = 4.7740(9) Å
CgI_perp = 3.3957(2) Å
α = 0.00(2)°
β = 44.7°
Offset = 3.356 Å

## Slide 20
Heteroaromatic rings:
N-methylpyridinium cations
Cg…Cg = 3.776(2) Å
CgI_perp = 3.766(2) Å
α = 0°
β = 4.2°
Offset = 0.279 Å
ρmax = 0.018 e Å-1

## Slide 21: Types of planar conjugated rings
aromatic
quinoid
semiquinoid
metal chelates

## Slide 22: More planar conjugated rings

## Slide 23: Quinoid rings: no more quadrupoles

## Slide 24: Netural quinones: tetrachloroquinone
ρmax = 0.080 e Å-1
ρmax = 0.042 e Å-1
3.13 Å
2.77 Å
Cg…Cg = 5.66 Å
CgI_perp = 3.17 Å
α = 0°
α = 68°

## Slide 25: Quinone anions: hydrogenchloranilate
Molčanov, Jelsch et al., CrystEngComm, 2015, 17, 8645.
ρmax = 0.059 e Å-1
E > 10 – 15 kcal mol-1
3.229(2) Å

## Slide 26
HCA-
HBA-
Effect of substituents
DHQ2-
Molčanov, Kojić-Prodić, Babić, Stare,CrystEngComm, 2013, 15, 135-143.

## Slide 27: Semiquinone radicals
Cl4Q
Br4Q
DDQ
X = Cl :
X = Br :
X = Cl, CN :
F4Q
X = F :
..

## Slide 28: Stacking of semiquinone radicals: spin coupling
200 K
Antiferromagnetic
3.27 Å
3.27 Å
3.58 Å
3.58 Å
3.46 Å
3.46 Å
3.46 Å
3.46 Å
Reversible!
Single crystal
to
Single crystal
CrystEngComm, 2012, 14, 7958-7964.
100 K
Diamagnetic

## Slide 29: Two polymorphs of N-MePy∙Cl4Q
0
a
b
c
0
c
b
a
triclinic
orthorhombic
Molčanov, Stilinović, Šantić, Maltar-Strmečki, Pajić, Kojić-Prodić, Cryst. Growth Des., 2016, 16, 4777-4782.

## Slide 30: N-MePy·Cl4Q, triclinic
2.903(1) Å
2.903(1) Å
3.663(1) Å
Peierls-type deformation
Dimers with coupled spins
Diamagnetic
Cryst. Growth Des., 2016, 16, 4777-4782.

## Slide 31: Interactions between the rings (diamagnet, dimer)
Offset: 2.07 Å
0.5 e Å-3
2.90 Å

## Slide 32: Interactions between the rings (diamagnet, between dimers)
Offset: 2.8 Å
0.5 e Å-3
3.66 Å

## Slide 33: Critical points (diamagnet)
2.90 Å
3.66 Å
(3, -1) bond
(3, +1) ring cenroid
(3, +3) cage centroid
ρmax > 0.095 e Å-3
ρmax < 0.040 e Å-3

## Slide 34
Interactions between the rings (diamagnet)
0.05 e Å-3
2.90 Å
3.66 Å

## Slide 35: N-MePy·Cl4Q, orthorhombic
3.283(1) Å
3.283(1) Å
3.283(1) Å
1D antiferromagnetic coupling in a stack
Semiconductor:
σ ≈ 10-6 ( cm)-1
EDC ≈ 0.34 eV
Cryst. Growth Des., 2016, 16, 4777-4782.

## Slide 36: Interactions between the rings (antiferromagnet)
Offset: 2.06 Å
0.5 e Å-3
3.28 Å

## Slide 37: Critical points (antiferromagnet)
3.28 Å
(3, -1) bond
(3, +1) ring cenroid
(3, +3) cage centroid
ρmax < 0.050 e Å-3

## Slide 38: Stacking geometry: dimer vs. equdistant stack
Offset: 2.07 Å
2.90 Å
3.28 Å
Offset: 2.06 Å
dimer
equidistant

## Slide 39: Conductivity?
2.90 Å
3.66 Å
2.90 Å
3.28 Å
3.28 Å
3.28 Å
e-
e-
e-
e-
e-
ΔE = 0.34 eV
huge ΔE
Isolator
Semiconductor

## Slide 40
Electric conductivity
Stacking direction
1 mm
Band gap, activation energy:
Possible electron „jumping” between the radicals
Energy barrier for the „jumping”
Possible application?

## Slide 41
Electric conductivity
Cl4Q∙N-MePy
Br4Q∙N-MePy
DDQ∙N-Me2Pic
vs. interplanar distance (100 K)
3.2855(16) Å
3.1587(13) Å
3.122(3) Å

## Slide 42
Inductive effect of the substituents
Cl4Q
Br4Q
DDQ
HOMO
HOMO
HOMO
LUMO
LUMO
LUMO
ΔE
ΔE
ΔE

## Slide 43
Direction of the offset
Molčanov, Babić, Kojić-Prodić, Stare, Maltar-Strmečki,
Androš Dubraja, Acta Cryst B., 2014, 70, 181-190.
Longitudinal offset
Transversal offset
LiDDQ·2H2O·MeCOEt
RbDDQ·2H2O
CsDDQ·2H2O

## Slide 44
Orientation of the stacked rings
Antiparallel
NaDDQ∙2H2O∙MeCOEt
Diamagnetic, isolator
Parallel
KDDQ∙H2O
Antiferromagnetic,
semiconductor
ΔE ≈ 2.4 kJ mol-1
Acta Cryst B., 2014, 70, 181-190; CrystEngComm, 2017, 19, 1801-1808.

## Slide 45
Orientation of the stacked rings
gauche
gauche
CsDDQ∙0.25H2O
Diamagnetic, isolator
Antiparallel
Antiparallel
Molčanov & Kojić-Prodić, CrystEngComm, 2017, 19, 1801-1808.

## Slide 46
Geometric parameters for description of stacking
Additional parameters for quinoid rings:
δ
∙
ε
Molčanov & Kojić-Prodić, CrystEngComm, 2017, 19, 1801-1808.

## Slide 47: Charge-transfer complexes
Mayerle, Torrance, Crowley, Acta Cryst. B, 1979, 35, 2988.
Lecomte et al., Faraday Discuss., 2007, 135, 271.
TTF∙Cl4Q
e-
δ+
δ+
δ+
δ–
δ–
δ–
A classical
example
≈ 3.60 Å

## Slide 48: Charge-transfer complexes
[N-Me-4-(Me)2NPy]2(Cl4Q)3
3.59 Å
2.84 Å
2.84 Å
1.32 Å
≈1.76 Å

## Slide 49: Charge-transfer complexes
[N-Me-4-(Me)2NPy]2(Cl4Q)3
2–
1+
1+
Charges derived from Pval:
–0,76
–0,58
–0,58
–1.92
+0.96
+0.96

## Slide 50: Charge-transfer complexes
2.84 Å
3.59 Å
ρmax > 0.077 e Å-3
ρmax < 0.045 e Å-3

## Slide 51: Metal-chelate rings: aromatic?
Jurić, Molčanov, Žilić, Kojić-Prodić, RSC Adv., 2016, 6, 62785-62796.
[Cu(CA)2(H2O)2]Him2

## Slide 52: Metal-chelate rings: aromatic?
[Cu(CA)2(H2O)2]Him2

## Slide 53: Metal-chelate rings: aromatic?
Cu1-O1
ρtot = 0.3520 e Å-3
Laplacian = 6.29
Cu1-O2
ρtot = 0.3898 e Å-3
Laplacian = 7.08
Cu-O bond critical points (3,-1):
Laplacian of electron density

## Slide 54: Stacking of metal-chelate rings in [Cu(CA)(2,2’-bpy)]
0
a
c
b
Jurić, Molčanov, Kojić-Prodić, Dalton Trans., 2013, 42, 15756-15765.

## Slide 55: Stacking of metal-chelate rings: chelate∙∙∙chelate, chelate∙∙∙aromatic and chelate∙∙∙quinone
Jurić, Molčanov, Kojić-Prodić, Dalton Trans., 2013, 42, 15756-15765.
Interplanar distance ≈ 3.28 Å
3.40 Å < Cg…Cg < 3.84 Å
α ≈ 2 °

## Slide 56: Stacking of metal-chelate rings: electrostatic potential
Jurić, Molčanov, Kojić-Prodić, Dalton Trans., 2013, 42, 15756-15765.

## Slide 57: Stacking of metal-chelate rings: Voronoi-Dirichlet polyhedra
Jurić, Molčanov, Kojić-Prodić, Dalton Trans., 2013, 42, 15756-15765.

## Slide 58: π-Stacking of the coordination polymers: [Cu(CA)(MeCN)]n
Jurić, Molčanov, Žilić, Kojić-Prodić, RSC Adv., 2016, 6, 62785-62796.
3.26 Å
offset:
≈ 1.6 Å

## Slide 59: π-Stacking of the coordination polymers: [Cu(CA)(MeCN)]n
Jurić, Molčanov, Žilić, Kojić-Prodić, RSC Adv., 2016, 6, 62785-62796.

## Slide 60: Stacking or bonding? [Cu(CA)(1,10’-phen)]
0
a
c
b
2.574(2) Å
≈ 3.2 Å
Jurić, Molčanov, Kojić-Prodić, Dalton Trans., 2014, 43, 7208-7218.

## Slide 61: Stacking or bonding? [Cu(CA)(1,10’-phen)]
Jurić, Molčanov, Kojić-Prodić, Dalton Trans., 2014, 43, 7208-7218.

## Slide 62: Cooperative stacking?
3.88 Å

## Slide 63: Anion∙∙∙π interactions?
Br4Q
N-Me-2-pic∙I∙Br4Q
e-
…with a partial charge transfer!
3.54 – 3.94 Å
70 – 80°
offset ≈ 1 Å

## Slide 64
Anion∙∙∙π interactions?
electrostatic potential
Voronoi-Dirichlet
polyhedra

## Slide 65: Conclusions
Closed-shell rings:
occur between all planar rings
dominantly electrostatic
stronger between rings with little or no π electron delocalisation
weak between fully delocalised systems
energy of interaction varies from < 1 kcal mol-1 to > 15 kcal mol-1
potential use in crystal engineering

## Slide 66: Conclusions
2) Radicals:
energy of interaction exceeds 15 kcal mol-1
dominant interaction is spin coupling (interplanar distance)
secondary: electrostatic (offset)
possible electron transfer between the rings: semiconductivity
magnetic properties can be tuned by tuning geometry of stacking

## Slide 67: Acknowlegdements
Croatian Science Foundation, grant no. IP-2014-09-4079
Croatian Academy of Sciences and Arts
French-Croatian bilateral, Slovenian-Croatian bilateral
Croatian Association of Crystallographers
RBI, Zagreb
Biserka Kojić-Prodić
Zoran Štefanić
Marijana Jurić
Lidija Androš Dubraja
Nadica Maltar-Strmečki
Ana Šantić
Dijana Žilić
Darko Babić
Valentina Milašinović
Lidija Kanižaj
Université de Lorraine
Christian Jelsch
Claude Lecomte
Emmanuel Wenger
University of Zagreb
Vladimir Stilinović
Damir Pajić
Nikolina Novosel
Krešo Zadro
Mario Cetina
University of Ljubljana
Anton Meden
KI, Ljubljana
Jernej Stare
Gregor Mali
Dušan Hadži
Jože Grdadolnik
Rigaku Oxford Diffraction Ltd.
Marcus Winter
Dyanne Cruikshank